Filters

Subsystem Specification Document

SPIRE Ref.: SPIRE-QMW-PRJ-000454

Cardiff Ref.: HSO-CDF-SP-002

Issue: 2.0

Prepared by: Peter Hargrave

Last Modified on: 23 August 2001

Approved by:

Distribution list

Update history

| Date | Version | Remarks |
| --- | --- | --- |
| 03 April 2000 | Draft 1.0 | First draft. No detailed design available. |
| 14 July 2000 | Issue 1.0 | First issue |
| 19 April 2001 | Issue 1.1 | Revised & updated for IIDR |
| 23 August 2001 | Issue 1.2 | Revised filter bands |
| 7/9/01 | 2.0 | First configuration controlled issue. |

List of Acronyms

| Term | Meaning | Term | Meaning |
| --- | --- | --- | --- |
| AD | Applicable Document | IR | Infrared |
| ADC | Analogue to Digital Converter | IRD | Instrument Requirements Document |
| AIV | Assembly, Integration and Verification | IRTS | Infrared Telescope in Space |
| AME | Absolute Measurement Error | ISM | Interstellar Medium |
| AOCS | Attitude and Orbit Control System | JFET | Junction Field Effect Transistor |
| APART | Arizona's Program for the Analysis of Radiation Transfer | ISO | Infrared Space Observatory |
| APE | Absolute Pointing Error | LCL | Latching Current Limiter |
| ASAP | Advanced Systems Analysis Program | LIA | Lock-In Amplifier |
| ATC | Astronomy Technology Centre, Edinburgh | LVDT | Linear Variable Differential Transformer |
| AVM | Avionics Model | LWS | Long Wave Spectrometer (an instrument used on ISO) |
| BDA | Bolometer Detector Array | MAC | Multi Axis Controller |
| BFL | Back Focal Length | MAIV | Manufacturing, Assembly, Integration and Verification |
| BRO | Breault Research Organization | MCU | Mechanism Control Unit = HSMCU |
| BSM | Beam Steering Mirror | MGSE | Mechanical Ground Support Equipment |
| CBB | Cryogenic Black Body | M-P | Martin-Puplett |
| CDF | Cardiff, Department of Physics & Astronomy | NEP | Noise Equivalent Power |
| CDMS | Command and Data Management System | NTD | Neutron Transmutation Doped |
| CDMU | Command and Data Management Unit | OBS | On-Board Software |
| CDR | Critical Design Review | OGSE | Optical Ground Support Equipment |
| CEA | Commissariat a l’Energie Atomique | OMD | Observing Modes Document |
| CMOS | Complimentary Metal Oxide Silicon | OPD | Optical Path Difference |
| CoG | Centre of Gravity | PACS | Photodetector Array Camera and Spectrometer |
| CPU | Central Processing Unit | PCAL | Photometer Calibration source |
| CQM | Cryogenic Qualification Model | PFM | Proto-Flight Model |
| CVV | Cryostat Vacuum Vessel | PID | Proportional, Integral and Differential (used in the context of feedback control loop architecture) |
| DAC | Digital to Analogue Converter | PLW | Photometer, Long Wavelength |
| DAQ | Data Acquisition | PMW | Photometer, Medium Wavelength |
| DCU | Detector Control Unit = HSDCU | POF | Photometer Observatory Function |
| DDR | Detailed Design Review | PROM | Programmable Read Only Memory |
| DM | Development Model | PSW | Photometer, Short Wavelength |
| DPU | Digital Processing Unit = HSDPU | PUS | Packet Utilisation Standard |
| DSP | Digital Signal Processor | RAL | Rutherford Appleton Laboratory, |
| DQE | Detective Quantum Efficiency | RD | Reference Document |
| EDAC | Error Detection and Correction | RMS | Root Mean Squared |
| EGSE | Electrical Ground Support Equipment | SCAL | Spectrometer Calibration Source |
| EM | Engineering Model | SCUBA | Submillimetre Common User Bolometer Array |
| EMC | Electro-magnetic Compatibility | SED | Spectral Energy Distribution |
| EMI | Electro-magnetic Interference | SMEC | Spectrometer Mechanics |
| ESA | European Space Agency | SMPS | Switch Mode Power Supply |
| FCU | FCU Control Unit = HSFCU | SOB | SPIRE Optical Bench |
| FIR | Far Infrared | SOF | Spectrometer Observatory Function |
| FIRST | Far Infra-Red and Submillimetre Telescope | SPIRE | Spectral and Photometric Imaging Receiver |
| FOV | Field of View | SRAM | Static Random Access Memory |
| F-P | Fabry-Perot | SSSD | SubSystem Specification Document |
| FPGA | Field Programmable Gate Array | STP | Standard Temperature and Pressure |
| FPU | Focal Plane Unit | SVM | Service Module |
| FS | Flight Spare | TBC | To Be Confirmed |
| FTS | Fourier Transform Spectrometer | TBD | To Be Determined |
| FWHM | Full Width Half maximum | TC | Telecommand |
| GSFC | Goddard Space Flight Center | URD | User Requirements Document |
| HK | House Keeping | UV | Ultra Violet |
| HOB | Herschel Optical Bench | WE | Warm Electronics |
| HPDU | Herschel Power Distribution Unit | ZPD | Zero Path Difference |
| HSDCU | Herschel-SPIRE Detector Control Unit |  |  |
| HSDPU | Herschel-SPIRE Digital Processing Unit |  |  |
| HSFCU | Herschel-SPIRE FPU Control Unit |  |  |
| HSO | Herschel Space Observatory |  |  |
| IF | Interface |  |  |
| IID-A | Instrument Interface Document - Part A |  |  |
| IID-B | Instrument Interface Document - Part B |  |  |
| IMF | Initial Mass Function |  |  |

Table of Contents

1.	Scope	6

2.	Documents	6

2.1.	Applicable documents	6

2.2.	Reference documents	6

3.	Subsystem Description	7

3.1.	Design philosophy and overview	7

3.2.	Photometer filtering scheme	8

3.2.1.	Comments on filtering scheme	8

3.3.	Spectrometer filtering scheme	11

4.	Specification of filter components	12

4.1.	Common filter	12

4.1.1.	CFIL1	12

4.2.	Photometer filters	12

4.2.1.	PFIL2	12

4.2.2.	PFIL3	13

4.2.3.	PDIC1	14

4.2.4.	PDIC2	15

4.2.5.	PFIL4S	16

4.2.6.	PFIL5S	16

4.2.7.	PFIL4M	16

4.2.8.	PFIL5M – Baseline – not implemented as edge defined by PDIC1	17

4.2.9.	PFIL4L	17

4.2.10.	PFIL5L – Baseline – not implemented as edge defined by PDIC2	17

4.2.11.	PFIL6L  Baseline – not implemented, since high-pass edge defined by waveguide cut-on.	18

4.3.	Spectrometer filters	18

4.3.1.	SFIL2	18

4.3.2.	SBS1	18

4.3.3.	SBS2	19

4.3.4.	SFIL3S	20

4.3.5.	SFIL4S	20

4.3.6.	SFIL5S	20

4.3.7.	SFIL6S Baseline – not implemented, since high-pass edge defined by waveguide cut-on.	21

4.3.8.	SFIL3L	21

4.3.9.	SFIL4L	21

4.3.10.	SFIL5L	22

4.3.11.	SFIL6L  Baseline – not implemented, since high frequency edge defined by waveguide cut-on.	22

5.	Functional requirements	22

5.1.	Technical constraints	22

6.	Design, manufacture & test requirements	23

6.1.	Design requirements	23

6.2.	Product assurance plan	23

6.3.	Parts, materials and processes	23

6.3.1.	General	23

6.3.2.	Materials, processes and mechanical parts approval and listing	24

6.3.3.	Cleanliness	24

6.3.4.	Finish	24

6.3.5.	Outgassing	24

6.3.6.	Materials selection	24

6.3.7.	Processes	24

7.	Operational requirements	24

7.1.	Safety	24

7.2.	Lifetime	24

7.3.	Operating modes	24

8.	Interface requirements	24

9.	Logistic requirements	25

9.1.	Storage	25

9.2.	Handling	25

9.3.	Transportation	25

9.4.	ESD precautions	25

10.	Environmental requirements	25

10.1.	Shock	25

10.2.	Vibration	25

10.3.	Vacuum level	25

10.4.	Vacuum outgassing	25

10.5.	Temperature	25

10.6.	Magnetic fields	25

10.7.	Survival temperature	25

10.8.	Radiation environment	26

11.	Verification requirements	26

11.1.	Performance requirements	26

11.2.	System Requirements	26

# Scope

This specification defines the requirements and specifications applied to the performance, design, qualification and interfaces of the SPIRE Filters subsystem. It is applicable to the STM, the CQM, the PFM and the FS as described in this document.

# Documents

## Applicable documents

All applicable documents are listed in the AD chapter of the CIDL (HSO-CDF-LI-029).

## Reference documents

# Subsystem Description

## Design philosophy and overview

The first filter in the chain, situated on the 4-K box, should reflect back to the sky as much unwanted high frequency radiation as possible. Filters on lower temperature shields should then reject radiation from higher temperature boxes and shields.

Strategic placement of filters will enable us to:

- Define the spectral passbands.

- Minimise the thermal loading on the 3He fridge, 2-K and 4-K stages by rejecting short wavelength thermal energy.

- Minimise stray light getting to the detectors.

- Maximise the in-band spectral transmission.

The layout of filters on SPIRE is shown schematically by Figure 1 and Figure 2.

Figure 1 Topology of photometer side of SPIRE. Filters and dichroics are shown in green.

Figure 2 Topology of spectrometer side of SPIRE. Filters and beam splitters are shown in green.

## Photometer filtering scheme

A summary of the photometer filter requirements is shown in Table 1.

The full specifications of each filter component are detailed in section 4.

### Comments on filtering scheme

These comments are also valid for the spectrometer filters.

Thickness:- The dimension shown in the column is the thickness of the filter itself, not including any mounting rings.

Size:- The numbers in this column define the minimum clear aperture (MCA) required. A single number represents the diameter of a circular aperture, and two numbers are the sides of a rectangular aperture.

Assumptions:-

For blocking filters, the 90 % and 10 % edges are within 5 % of the 50 %  transmission point. 2 % blocking is achieved at 10cm-1 away from the 50 % point.

For the dichroics, the 50 % point in reflection is separated by 0.6 cm-1 from the 50 % point in transmission.

Definition of tolerance:-

% transmission is with respect to the peak

Blocking, B, refers to blocking at <2 %.

50 % edge has a tolerance of ( 1 % in frequency.

10 % and 9 0% edges shall be within the values specified.

In-band transmission:-

The overall transmission of the filter stack has a design value of >60 %, averaged over the central 50 % of the band.

| 50% bands (m) as determined by these filters: |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | o |  |  |  |  |  |  |  |
| P/SW | 208.3 | - | 300.3 | 2.77 |  | 254 |  | But waveguide cut-off limits it to 291.7 |  |
| P/MW | 305.8 | - | 420.2 | 3.17 |  | 363 |  | Waveguide cut-off is set at 420.0 |  |
| P/LW | 431.0 | - | 583.3 | 3.33 |  | 507 |  | Note: 583.3 is set by waveguide cut-off |  |

| 50% bands (m) as specified in feedhorn design |  |  |
| --- | --- | --- |
|  |  |  |  |  |  | o |  |  |
| P/SW | 208.3 | - | 291.7 | 3.00 |  | 250 |  | OK |
| P/MW | 306.0 | - | 420.1 | 3.18 |  | 363 |  | OK |
| P/LW | 416.7 | - | 583.3 | 3.00 |  | 500 |  | Band defined by the current filters/dichroics is narrower. |
|  |  |  |  |  |  |  |  | Options: keep bandwidth of 3.3 or else open out LW waveguide. |

Table 1 Photometer filters and dichroics.

## Spectrometer filtering scheme

Table 2 Spectrometer filters and beam dividers

# Specification of filter components

This section lists the specifications for the SPIRE filters. All interface details are contained in the filters ICD (HSO-CDF-ICD-012).

## Common filter

### CFIL1

This filter covers the entrance aperture to the SPIRE 4-K box, and will be rectangular in format. It is a common input filter for both the photometer and spectrometer.

Table 3 CFIL1 details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 135x67 mm MCA, outer dimensions TBC |
| Interface | Clamp ring |
| Mass | 5 g TBC |
| Spectral characteristics | LPE 100 cm-1 |
| Comments |  |

## Photometer filters

### PFIL2

This filter covers an aperture in the baffle, PBFL2, in the photometer box, and is only seen by the photometer detectors. A general mounting sketch is shown in Figure 3.

Table 4 PFIL2 details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 76 mm MCA |
| Interface | Clamp ring |
| Mass | 3 g TBD |
| Spectral characteristics | LPE 90 cm-1 |
| Comments |  |

Figure 3 Sketch showing the mounting concept to be used for all circular hot-pressed filter components. Detailed drawings for all hot-pressed filters and mounts are in progress at the time of writing of this issue.

### PFIL3

This filter covers the 2-K cold stop in the photometer.

Table 5 PFIL3 details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | TBD |
| Interface | Clamp ring |
| Mass | 3 g TBC |
| Spectral characteristics | LPE 60 cm-1 |
| Comments |  |

### PDIC1

This is the first dichroic in the photometer chain. It is essential that this component remains flat upon cooling, and so it has to be mounted on a substantial ring. An assembly drawing for PDIC1 is shown in Figure 4. This drawing is awaiting approval at the time of writing this document.

Table 6 PDIC1 details

| Type | Hot Pressed (TBD), Ring mounted |
| --- | --- |
| Dimensions | 80mm MCA, 94 mm o/d, 13.5 mm depth |
| Interface | 3-point mounting ring |
| Mass | 287 g TBC |
| Spectral characteristics | LPE 32.7 cm-1 (to give a HPE in reflection of 33.3 cm-1) |
| Comments | The mass of this component may be reduced after prototype tests have been completed. This component must remain flat, and therefore needs a substantial ring mount. |

Figure 4 Assembly drawing for PDIC1

### PDIC2

This is the second dichroic in the photometer chain. It is essential that this component remains flat upon cooling, and so it has to be mounted on a substantial ring. An assembly drawing for PDIC2 is shown in Figure 5. This drawing is awaiting approval at the time of writing this document.

Table 7 PDIC2 details

| Type | Hot Pressed (TBD), Ring mounted |
| --- | --- |
| Dimensions | 75 mm i/d, 90 mm o/d (MCA=72mm) |
| Interface | 3-point mounting ring |
| Mass | 250 g TBC |
| Spectral characteristics | LPE 23.2 cm-1 (to give a HPE in reflection of 23.8 cm-1) |
| Comments | The mass of this component may be reduced after prototype tests have been completed. This component must remain flat, and therefore needs a substantial ring mount. |

Figure 5 Assembly drawing for PDIC2

### PFIL4S

This filter is fitted to the SW BDA at 300-mK.  Blocker over SW array.

Table 8 PFIL4S details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 31x56 mm (25x50 mm MCA) |
| Interface | Clamp ring |
| Mass | 1.5 g |
| Spectral characteristics | LPE 50 cm-1 |
| Comments | Clamps to detector module. |

### PFIL5S

This filter is fitted to the SW BDA at 300-mK. Low-pass edge-definer over SW array.

Table 9 PFIL5S details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 31x56 mm (25x50mm MCA) |
| Interface | Clamp ring |
| Mass | 1.5 g |
| Spectral characteristics | LPE 48 cm-1 |
| Comments | Clamps to detector module. |

### PFIL4M

This filter is fitted to the MW BDA at 300-mK. Blocker over MW array.

Table 10 PFIL4M details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 31x56 mm (25x50 mm MCA) |
| Interface | Clamp ring |
| Mass | 1.5 g |
| Spectral characteristics | LPE 43 cm-1 |
| Comments | Clamps to detector module. |

### PFIL5M – Baseline – not implemented as edge defined by PDIC1

This filter is fitted to the MW BDA at 300-mK.  Low-pass edge-definer for MW array.

Table 11 PFIL5M details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 31x56mm (25x50mm MCA) |
| Interface | Clamp ring |
| Mass | 1.5g |
| Spectral characteristics | LPE 33.0cm-1 |
| Comments | Clamps to detector module. |

### PFIL4L

This filter is fitted to the LW BDA at 300-mK. Blocker over LW array.

Table 12 PFIL4L details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 31x56 mm (25x50 mm MCA) |
| Interface | Clamp ring |
| Mass | 1.5 g |
| Spectral characteristics | LPE 30 cm-1 |
| Comments | Clamps to detector module. |

### PFIL5L – Baseline – not implemented as edge defined by PDIC2

This filter is fitted to the LW BDA at 300-mK.  Low-pass edge-definer for LW array

Table 13 PFIL5L details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 31x56mm (25x50mm MCA) |
| Interface | Clamp ring |
| Mass | 1.5g |
| Spectral characteristics | LPE 23.2cm-1 |
| Comments | Clamps to detector module. |

### PFIL6L  Baseline – not implemented, since high-pass edge defined by waveguide cut-on.

High-pass edge-definer over LW array.

Table 14 PFIL6L details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 31x56mm (25x50mm MCA) |
| Interface | Clamp ring |
| Mass | 1.5g |
| Spectral characteristics | HPE 17.2cm-1 |
| Comments | Clamps to detector module. This filter may be needed to define the high-pass cut-on for the long wavelength channel (the dichroics define the HPE for the other two channels) |

## Spectrometer filters

### SFIL2

This filter is positioned at the pupil in the SPIRE optical bench.

Table 15 SFIL2 details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 30 mm MCA, 36 mm o/d (TBC) |
| Interface | Clamp ring |
| Mass | 1 g |
| Spectral characteristics | LPE 90 cm-1 |
| Comments |  |

### SBS1

This component must remain flat, and therefore it shall be ring mounted. An assembly drawing is shown in Figure 6.

Table 16 SBS1 details

| Type | Hot Pressed (TBC), Ring mounted |
| --- | --- |
| Dimensions | 46 mm i/d, 56 mm o/d, 38 mm MCA (TBC) |
| Interface | 3-point mounting ring |
| Mass | 32 g |
| Spectral characteristics | 15-50 cm-1 beam splitter |
| Comments | Size 5 ring |

Figure 6 Assembly drawing of SBS1 and SBS2.

### SBS2

This component must remain flat, and therefore it shall be ring mounted. An assembly drawing is shown in Figure 6. Mounted in opposition to SBS1 – critical.

Table 17 SBS2 details

| Type | Hot Pressed (TBC), Ring mounted |
| --- | --- |
| Dimensions | 46 mm i/d, 56 mm o/d, 38 mm MCA (TBC) |
| Interface | 3-point mounting ring |
| Mass | 32 g |
| Spectral characteristics | 15-50 cm-1 beam splitter |
| Comments | Size 5 ring |

### SFIL3S

This filter covers the 2-K cold stop at the entrance to the SW side of the spectrometer detector box.

Table 18 SFIL3S details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 40 mm MCA, 43 mm o/d – |
| Interface | Clamp ring |
| Mass | 1 g |
| Spectral characteristics | LPE 70 cm-1 |
| Comments |  |

### SFIL4S

This filter is fitted to the SW spectrometer BDA at 300-mK.

Table 19 SFIL4S details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 16 mm MCA, o/d TBD |
| Interface | Clamp ring |
| Mass | 1 g |
| Spectral characteristics | LPE 60 cm-1 |
| Comments | Blocker |

### SFIL5S

This filter is fitted to the SW spectrometer BDA at 300-mK.  Low-pass edge definer for the LW band.  Filter designed to give the 90% power point at 50cm-1.

Table 20 SFIL5S details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 16 mm MCA, o/d TBD |
| Interface | Clamp ring |
| Mass | 1 g |
| Spectral characteristics | LPE 52.6 cm-1 |
| Comments | Edge definer |

### SFIL6S Baseline – not implemented, since high-pass edge defined by waveguide cut-on.

This filter is fitted to the SW spectrometer BDA at 300-mK.  High-pass edge-definer for SW band.

Table 21 SFIL6S details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 16 mm MCA, o/d TBD |
| Interface | Clamp ring |
| Mass | 1 g |
| Spectral characteristics | HPE 30.8 cm-1 |
| Comments | Designed to allow for a 10um overlap between the SW and LW bands. |

### SFIL3L

This filter covers the 2-K cold stop at the entrance to the LW side of the spectrometer detector box.

Table 22 SFIL3L details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 40 mm MCA, TBD o/d |
| Interface | Clamp ring |
| Mass | 1 g |
| Spectral characteristics | LPE 60 cm-1 |
| Comments |  |

### SFIL4L

This filter is fitted to the LW spectrometer BDA at 300-mK.

Table 23 SFIL4L details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 20 mm MCA, o/d TBD |
| Interface | Clamp ring |
| Mass | 1 g |
| Spectral characteristics | LPE 43 cm-1 |
| Comments | Blocker |

### SFIL5L

This filter is fitted to the LW spectrometer BDA at 300-mK.  Low-pass edge-definer for LW band.

Table 24 SFIL5L details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 20 mm MCA, o/d TBD |
| Interface | Clamp ring |
| Mass | 1 g |
| Spectral characteristics | LPE 33.4 cm-1 |
| Comments | Designed to allow for a 10 um overlap between the SW and LW bands. |

### SFIL6L  Baseline – not implemented, since high frequency edge defined by waveguide cut-on.

This filter is fitted to the LW spectrometer BDA at 300-mK.  High-pass edge definer for LW band.

Table 25 SFIL6L details

| Type | Hot Pressed |
| --- | --- |
| Dimensions | 20 mm MCA, o/d TBD |
| Interface | Clamp ring |
| Mass | 1 g |
| Spectral characteristics | HPE 14.2 cm-1 |
| Comments |  |

# Functional requirements

## Technical constraints

Table 26 Performance requirements on the filters sub-system. These requirements are extracted from AD11. The requirements shown in red appeared in a previous version of AD11, and may now be obsolete (TBC).

| Requirement ID | Description | Value |
| --- | --- | --- |
| IRD-PHOT-R01 | Nominal pass band | 250 mm, 350 mm and 500 mm (TBC) (/(( = 3 |
| IRD-SPEC-R01 | Wavelength range | Band 1 = 200-300mm, 31.15 - 50.0cm-1 (TBC) Band 2 = 300-670mm, 14.9 - 32.15cm-1 (TBC) |
| IRD-OPTP-R05 | Throughput | The throughput of the photometer mirrors, filters, dichroics and baffles shall be greater than 0.27 (TBC) over the instrument waveband. This includes losses due to manufacturing defects; surface finish and alignment tolerances. |
| IRD-OPTP-R07 | Out-of-band radiation | The end to end filtering of the photometer shall control the out of band radiation to be no more than 10-3 for 50 cm-1 to 200 cm-1 10-6 for 200 cm-1 to 1000 cm-1 10-9 for 1000 cm-1 to 100000 cm-1 of the in-band telescope background radiation. |
| IRD-OPTS-R05 | Throughput | The theoretical throughput of the spectrometer mirrors; filters; beam splitters and baffles shall be greater than 0.2 (TBC) over the total instrument waveband (TBC) including all losses due to manufacturing defects; surface finish and alignment tolerances. |
| IRD-OPTS-R07 | Balancing of ports | In order that the two output ports shall have the same performance and to facilitate accurate compensation of the zero path difference maximum, the beam splitters shall have 2RT equal to R2 +T2 to within 90% (TBC) over the waveband of the instrument. |
| IRD-OPTS-R08 | Out-of-band radiation | The end-to-end filtering of the spectrometer shall control the out of band radiation to be no more than 10-3 for 50 cm-1 to 200 cm-1 10-6 for 200 cm-1 to 1000 cm-1 10-9 for 1000 cm-1 to 100000 cm-1 of the in-band telescope background radiation. |

# Design, manufacture & test requirements

## Design requirements

Cardiff University design procedures shall be followed.

## Product assurance plan

The deliverables from the filters, beam splitters and dichroics work-package will comply with the SPIRE product assurance plan (AD12) and with the Cardiff internal product assurance plan (AD30).

## Parts, materials and processes

### General

The workmanship and materials used shall be, or shall be shown to be compatible in any future build, of a standard consistent with flight hardware. The number of materials, mechanical parts types, and processes shall be minimized. Materials and mechanical parts that have been successfully used in similar space applications shall be preferred. Standard processes or known processes previously used in space applications shall be preferred. Material justification shall prove the hardware structural integrity during the design life.

### Materials, processes and mechanical parts approval and listing

All MPM meeting the requirements of this document shall be approved by submitting to SPIRE PA the Declared Materials List. If these requirements are not met, a RFA shall be submitted to ESA. A Declared Materials List (DML) shall be drawn up, according to the requirements of ECSS-Q- 70 § 3.1.3. Materials with limited-life characteristics and non-metallic materials shall be highlighted. Mechanical parts shall be included in the DML as a separate group. Process details shall also be included in the DML for the appropriate material. Critical processes shall be highlighted.

### Cleanliness

All filters will be assembled in class 100 conditions.

### Finish

Surface finish shall prevent deterioration from exposure to the environment. Mechanical parts made of stainless steel shall be passivated.

### Outgassing

PSS-01-702 shall be used as a guideline.

### Materials selection

ESA and NASA guidelines will be followed. No materials will be used that have not already been flown on previous space missions.

### Processes

The use of existing ESA documents shall be maximized where appropriate. Critical processes shall be identified and reported to TBD through a critical process list or the DML.

# Operational requirements

## Safety

N/A

## Lifetime

The lifetime of the filters shall be at least 5 years in orbit and 5 years on ground.

## Operating modes

N/A

# Interface requirements

All 4-K and 2-K filters interface with the SPIRE structure, and the interface is defined in the Filters ICD (AD28).

All 300-mK filters interface with the BDAs. This interface is still to be defined.

# Logistic requirements

## Storage

The filters shall not suffer any performance degradation following storage in a dry nitrogen atmosphere for a period of up to 5 years.

Storage temperatures shall be in the range +5°C to +30°C.

## Handling

Ring mounted components (beam splitters and dichroics) must only be handled and installed by suitably trained staff from the Cardiff filter group. Suitably trained staff may handle other filter components, following procedures specified by Cardiff (TBW).

## Transportation

TBW

## ESD precautions

N/A

# Environmental requirements

These requirements are imposed by the environment the subsystem will encounter during its life.

## Shock

A working figure of 50g static acceleration loads in all three axes is assumed for all filter components. The actual levels are TBD.

## Vibration

TBD

## Vacuum level

Less than 10-4 Pa TBC

## Vacuum outgassing

Less than TBC

## Temperature

The filters will perform to specification at their intended temperatures, depending on their position in SPIRE (4-K box, 2-K box or 300-mK detectors).

## Magnetic fields

N/A

## Survival temperature

The filters, beam splitters and dichroics shall remain unaffected by exposure to temperatures of 80(C for periods of up to 72 hours.

## Radiation environment

Look up ISO & Cassini figures – estimate change for L2 environment

# Verification requirements

The filters development plan (RD2) contains more detail on the actual tests to be carried out. The tables below show how each of the functional and operational requirements in this document are to be demonstrated for each of the filter sets for the SPIRE models.

## Performance requirements

Test 			T

Measurement	M (Spectroscopy – FIR – UV)

Analysis 		A

Inspection 		I

| Requirement ID | Description | CQM | PFM | FS |
| --- | --- | --- | --- | --- |
| IRD-PHOT-R01 | Nominal pass band | M | M | M |
| IRD-SPEC-R01 | Wavelength range | M | M | M |
| IRD-OPTP-R05 | Throughput | M | M | M |
| IRD-OPTP-R07 | Out of band radiation | M | M | M |
| IRD-OPTS-R05 | Throughput | M | M | M |
| IRD-OPTS-R07 | Balancing of ports | M | M | M |
| IRD-OPTS-R08 | Out of band radiation | M | M | M |

## System Requirements

To be written.

# Comments

Can use Cassini polariser ring (cas15-1.dwg)

Can use Polariser #1 ring.

# Text boxes

Recess in structure to take filter

Clamp ring