|  | FIRST SPIRE | Ref : SPIRE-PRJ-000454 Author : P. Hargrave | Page : 1 / 1 Date : 14 June 2000 |
| --- | --- | --- | --- |
| SPIRE Filters subsystem specification |

Issue 1.0

Distribution List :

| RAL | K.King |  |  |  |
| --- | --- | --- | --- | --- |
|  | B.M.Swinyard |  |  |  |
| ATC | C.Cunningham |  |  |  |
| QMW | M.J.Griffin |  |  |  |
|  | P.A.R.Ade |  |  |  |
|  | C.V.Haynes |  |  |  |
|  | C.E.Tucker |  |  |  |

_________________________________________________________________________________

Queen Mary & Westfield College, Astrophysics Laboratory, Mile End Road, London E1 4NS

Tel. +44 (20) 7415 3757  Fax. +44 (20) 8980 0986

Update

| Date | Indice | Remarks |
| --- | --- | --- |
| 03 April 2000 |  | Creation of the document |
| 14 July 2000 |  | Issue 1.0 |

| Host system | Windows NT 4.0 |
| --- | --- |
| Word Processor | Microsoft Word 2000 |
| File | G:\Projects\First\Spire\Management\Documents\Sub_sys_Spec_docs\Spire Filters subsystem specification.doc |

Table of contents

1.	Scope of the document	5

2.	Documents	5

2.1.	Applicable documents	5

2.2.	Glossary	5

3.	Subsystem description	5

3.1.	Design philosophy	5

3.2.	Filter design – vacuum gap filters – to be completed	6

3.3.	Filter design – dielectric gap filters – to be completed	6

3.4.	Photometer filtering scheme	7

3.5.	Spectrometer filtering scheme	9

4.	Specification of filter components	10

4.1.	Common filters	10

4.1.1.	CFIL1	10

4.1.2.	CFIL2	10

4.2.	Photometer filters	10

4.2.1.	PFIL3	10

4.2.2.	PDIC1	10

4.2.3.	PDIC2	10

4.2.4.	PFIL4S	11

4.2.5.	PFIL4M	11

4.2.6.	PFIL4L	11

4.2.7.	PFIL5S	11

4.2.8.	PFIL5M	11

4.2.9.	PFIL5L	11

4.3.	Spectrometer filters	12

4.3.1.	SBS1	12

4.3.2.	SBS2	12

4.3.3.	SFIL3A	12

4.3.4.	SFIL3B	12

4.3.5.	SFIL4S	12

4.3.6.	SFIL4L	12

4.3.7.	SFIL5S	13

4.3.8.	SFIL5L	13

5.	Requirements	13

5.1.	Performance requirements	13

5.2.	Technical requirements – to be completed	14

5.3.	Operational requirements – to be completed	15

5.3.1.	Operational Safety	15

5.3.2.	Lifetime	15

5.4.	Interface requirements	15

5.5.	Design and manufacture requirements	15

5.5.1.	Design requirements	15

5.5.2.	Design rules	15

5.5.3.	Manufacture requirements	16

5.6.	Logistics – to be completed	16

5.6.1.	Packaging	16

5.6.2.	Transport and handling	16

5.6.3.	Storage	16

5.7.	Environment – to be completed	16

5.7.1.	Natural environment	16

5.7.2.	Operating environment	16

5.8.	Verification requirements – to be completed	16

# Scope of the document

This document defines the optical filtering scheme for the SPIRE instrument. It is applicable to the CQM, the PFM and the FS. It concentrates solely on the filters, beam splitters and dichroics needed for the photometer and spectrometer. The following topics are covered by this document:

- The general design philosophy

- The scientific requirements for the filtering

- The filtering specifications for the photometer and spectrometer

- The manufacturing procedures and QC/QA for filter production

- Risk analysis and testing procedures

The issue of filter mounting and integration is covered by document AD2, and work breakdown and scheduling is covered by document AD3

# Documents

## Applicable documents

|  | Title | Author | Reference | Date |
| --- | --- | --- | --- | --- |
| AD1 | Instrument Requirements Document | B.M.Swinyard | SPIRE-RAL-PRJ-000034 Issue 0.21 | 30 Nov. 1999 |
| AD2 | Interface Control Document – Structure/Filters | P.Hargrave, B.Winter | SPIRE/ICD/1.1/1.2.1 Issue 1.0 | 13 June 2000 |
| AD3 | SPIRE instrument – Filters subsystem development plan | P.Hargrave | TBC | May 2000 |

## Glossary

| AD | Applicable Document |  |  |
| --- | --- | --- | --- |
|  |  | MGSE | Mechanical Ground Support Equipment |
| CDR | Critical Design Review |  |  |
|  |  | NA | Not Applicable |
| CoG | Center of Gravity | OGSE | Optical Ground Support Equipment |
| CQM | Cryogenic Qualification Model | PFM | ProtoFlight Model |

# Subsystem description

## Design philosophy

The first filter in the chain, situated on the 4-K box, should reflect back to the sky as much unwanted high frequency radiation as possible. Filters on lower temperature shields should then reject radiation from higher temperature boxes and shields.

Strategic placement of filters will enable us to:

- Define the spectral passbands.

- Minimise the thermal loading on the 3He fridge, 2-K,  and 4-K stages by rejecting short wavelength thermal energy.

- Minimise stray light getting to the detectors.

- Maximise the in-band spectral transmission.

## Filter design – vacuum gap filters – to be completed

Figure 1 Schematic showing filter construction method

## Filter design – dielectric gap filters – to be completed

## Photometer filtering scheme

Table 1 List of photometer filters and dichroics

| Specifications of photometer filters and dichroics |
| --- |
| Component ID | Temp (K) | Location | Type | Edges (cm-1) | Minimum clear aperture (mm) | Comments |
| CFIL1 | 4 | On 4-K box. Exact location TBD | Edge filter | 10% 105 50% 100 90% 95 | TBD. Depends on location. |  |
| CFIL2 | 4 | TBD | Edge filter | 10% 84 50% 80 90% 76 | 70 x 150 |  |
| PFIL3 | 2 | Pupil between POFR2 and POFR3 | Edge filter | 10% 74 50% 70 90% 66 | 45 dia. (Pupil is 41 x 44 inc. 20% oversize) |  |
| PDIC1 | 2 | After POFR3 | Low Pass Dichroic | 10% 40 50% 37 90% 34 | 90 dia. TBC | Transmits long ( |
| PDIC2 | 2 | After PDIC1 | Low Pass Dichroic | 10% 27 50% 25 90% 23 | 90 dia. TBC | Transmits long ( |
| PFIL4S | 0.3 | At SW array | Low pass edge High pass edge | 53 38 | 40 dia. (Field is 19 x 38) |  |
| PFIL4M | 0.3 | At MW array | Low pass edge High pass edge | 36 25.7 | 40 dia. |  |
| PFIL4L | 0.3 | At LW array | Low pass edge High pass edge | 24 17 (if necessary) | 40 dia. |  |
| PFIL5S | 0.3 | At SW array | Edge filter | 10% 70 50% 66 90% 62 | 40 dia. |  |
| PFIL5M | 0.3 | At MW array | Edge filter | 10% 46 50% 43 90% 40 | 40 dia. |  |
| PFIL5L | 0.3 | At LW array | Edge filter | 10% 27 50% 26 90% 25 | 40 dia. |  |

Figure 2 Photometer optics and filter locations

## Spectrometer filtering scheme

Table 2 List of spectrometer filters and beam dividers

| Specifications of FTS filters and beam dividers |
| --- |
| Component ID | Temp (K) | Location | Type | Edges (cm-1) | Clear aperture (mm) | Comments |
| CFIL1 | 4 | On entrance to 11-K box | Edge filter | 10% 105 50% 100 90% 95 | 70 x 150 (Beam fooTprint on CIPM is 54 x 132) | Shared with photometer |
| CFIL2 | 4 | Above M3 | Edge filter | 10% 84 50% 80 90% 76 | 70 x 150 | Shared with photometer |
| SBS1 | 4 | After SIRM | Beam divider | 15 to 60 >90% 4RT | 36 dia. |  |
| SBS2 | 4 | After SDCM-A or -B | Beam divider | 15 to 60 >90% 4RT | 36 dia |  |
| SFIL3S SFIL3L | 2 | After SCAM-A or SCAM-B | Edge filter | 10% 74 50% 70 90% 66 | 40 dia. |  |
| SFIL4S | 0.3 | At SW array | Low pass edge High pass edge | 50 33 | 15 |  |
| SFIL4L | 0.3 | At LW array | Low pass edge High pass edge | 33 None ? | 15 |  |
| SFIL5S | 0.3 | At SW array | Edge | 10% 70 50% 66 90% 62 | 15 |  |
| SFIL5L | 0.3 | At LW array | Edge | 10% 46 50% 43 90% 40 | 15 |  |

Figure 3 Spectrometer optics and filtering scheme

## Specification of filter components

### Common filters

### CFIL1

Type				Hot Pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 100cm-1

Comments	Location and dimensions of this filter will be specified once the structure CAD model has been integrated with the optical beams.

### CFIL2

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 80cm-1

Comments	Location and dimensions of this filter will be specified once the structure CAD model has been integrated with the optical beams.

### Photometer filters

### PFIL3

Type				Hot pressed

Dimensions			54mm diameter. 1mm(TBC) thick.

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 70cm-1

Comments	Located at cold stop on 2-K box.

### PDIC1

Type				Hot pressed on ring.

Dimensions			Ring dimensions - 95mm o/d, 80mm i/d, 11mm thick

Interface			Ring mounted. Need three-point mount.

Mass				TBD

Spectral characteristics		Low pass dichroic. Transmits below 37cm-1, reflects above 37cm-1.

Comments			This component must be ring mounted to keep it flat.

This component is of a non-standard ring size. QMW will re-tool as necessary.

### PDIC2

Type				Hot pressed on ring.

Dimensions			Ring dimensions - 85mm o/d, 72mm i/d, 11mm thick

Interface			Ring mounted. Need three-point mount.

Mass				TBD

Spectral characteristics		Low pass dichroic. Transmits below 25cm-1, reflects above 25cm-1.

Comments			This component must be ring mounted to keep it flat.

This component is also of a non-standard ring size. However, it may be possible to use a QMW polarizer ring (90mm o/d, 75mm i/d).

### PFIL4S

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 53cm-1, HPE 38cm-1

Comments	Located at SW array.

It may be possible to dispense with the high pass edge, depending on the performance of the feedhorn waveguides.

### PFIL4M

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 36cm-1, HPE 25.7cm-1

Comments	Located at MW array.

It may be possible to dispense with the high pass edge, depending on the performance of the feedhorn waveguides.

### PFIL4L

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 24cm-1, HPE 17cm-1

Comments	Located at LW array.

It may be possible to dispense with the high pass edge, depending on the performance of the feedhorn waveguides.

### PFIL5S

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 66cm-1

Comments	Located at SW array.

### PFIL5M

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 43cm-1

Comments	Located at MW array.

### PFIL5L

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 26cm-1

Comments	Located at LW array.

### Spectrometer filters

### SBS1

Type				TBD on ring.

Dimensions			Ring dimensions - 46mm o/d, 38mm i/d, TBDmm thick

Interface			Ring mounted. Need three-point mount.

Mass				TBD

Spectral characteristics		>90% 4RT from 15cm-1 to 60cm-1

Comments			Non-standard ring size. QMW will re-tool as necessary.

### SBS2

Type				TBD on ring.

Dimensions			Ring dimensions - 46mm o/d, 38mm i/d, TBDmm thick

Interface			Ring mounted. Need three-point mount.

Mass				TBD

Spectral characteristics		>90% 4RT from 15cm-1 to 60cm-1

Comments			Non-standard ring size. QMW will re-tool as necessary.

### SFIL3A

Type				Hot pressed

Dimensions			43mm diameter (TBC).

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 70cm-1

Comments	Located at entrance to 2-K box.

The dimensions of this filter are likely to change. The present structure allows for a 1.5mm lip to clamp this filter. This is not enough.

### SFIL3B

Type				Hot pressed

Dimensions			43mm diameter (TBC).

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 70cm-1

Comments	Located at entrance to 2-K box.

The dimensions of this filter are likely to change. The present structure allows for a 1.5mm lip to clamp this filter. This is not enough.

### SFIL4S

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 50cm-1, HPE 33cm-1

Comments	Located at SW array.

### SFIL4L

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 33cm-1

Comments	Located at LW array.

### SFIL5S

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 66cm-1

Comments	Located at SW array.

### SFIL5L

Type				Hot pressed

Dimensions			TBD

Interface			Clamp ring

Mass				TBD

Spectral characteristics		LPE 43cm-1

Comments	Located at LW array.

# Requirements

## Performance requirements

Table 3 Scientific and performance requirements specified in [AD1]

| Requirement | Implementation |
| --- | --- |
| IRD-PHOT-R01 | Nominal passband 250 mm, 350 mm and 500 mm (TBC) (/(( = 3 | For each photometer channel, the passband will be defined by the use of low pass filters, band splitting dichroics and band-defining filters |
| IRD-SPEC-R01 | Wavelength range Band A = 200-300mm, 33-50cm-1 (TBC) Band B = 300-670mm, 15-33cm-1 (TBC) | The spectrometer wavelength bands shall be defined by the use of low pass and high pass edge filters. |
| IRD-OPTP-05 | Overall optical efficiency: Greater than 0.27 | A pessimistic estimate of combined filter stack throughput, including all filter losses (scattering, diffraction etc.), is around 0.4 |
| IRD-OPTP-R07 | Out of band radiation: Requirement TBD until telescope optical properties defined | Out of band rejection estimates: –10-3 for 40 cm-1 to 200 cm-1 –10-6 for 200 cm-1 to 1000 cm-1 –10-9 for 1000 cm-1 to 100000 cm-1 Achieved by a combination of blockers with edges chosen to block harmonic leaks. Note: detectors, optics and telescope all enhance cut-off; for filters only, the above rejection estimates change to 10-3, 10-5 and 10-8 respectively. |

Figure 4 Example showing the definition of a 350 micron photometer channel using real filters developed at QMW. The passband ((/(() in this case is 3.

Figure 5 Blocking of out-of-band radiation out to 105 cm-1 for the filter combination shown in figure 4.

## Technical requirements – to be completed

These requirements are design dependent.

Typical list:

- Axis reference system

- Alignment constraint

- Field view

- Dimensions

- Center of gravity, mass, inertia

- Stiffness

## Operational requirements – to be completed

### Operational Safety

Typical list:

- Availability

- Reliability

- Maintenance

- Security

### Lifetime

Durations of

- Storage

- Life once integrated

- Life when operational

| # | Parameter | Value | IRD | Note |
| --- | --- | --- | --- | --- |
| OL1 | Ground Storage lifetime | 1 year | TBD | A guess |
| OL2 | Integrated lifetime | 3 years | TBD | About |
| OL3 | Ground operational lifetime | 4 years | TBD | Including all acceptance testing |
| OL4 | On orbit operational lifetime | >4.25 years | TBD | Operating during 1/6 of the mission duration (4.25 years) |

## Interface requirements

This will be completed once the structure and optics design is finalised.

List of all the interface constraints between the subsystem and the other subsystems in relation with it.

Typical list:

- Mechanical

- Thermal

- Optics

- Test equipment

This list must be compliant with the interface document if it exists. When an interface document exists, it must be in the list of the Applicable Documents.

## Design and manufacture requirements

### Design requirements

This will be completed once the structure and optics design is finalised.

### Design rules

General rules (nomalisation, standards )  and specific rules applicable for the subsystem design

### Manufacture requirements

This will be completed once the structure and optics design is finalised.

Requirements related to the accessibility, the integration/disintegration and ability to test the subsystem.

## Logistics – to be completed

### Packaging

Hot pressed filters will be sealed in poly-bags in a clean room environment.

Vacuum gap components will be packaged …..

### Transport and handling

The subsystem will be transported to and from RAL, MSSL and QMW.

The containers will have to guarantee that…..

### Storage

## Environment – to be completed

### Natural environment

This is the description of the natural environment of the subsystem during its life.

### Operating environment

This is the description of the environment imposed by the location of the subsystem in SPIRE and in FIRST.

Typical list :

- Mechanical environement : vibration levels, shocks, microvibrations, static loads, acoustic loads, etc...

- Thermal environment : Solar fluxes, inetrface temperature levels, etc...

- EMC environment

## Verification requirements – to be completed

Description of the verification means to be used to demonstrate that the subsystem is compliant with all the specifications listed in this document.

Typical list :

- Mathematical modelling

- Qualification tests

- Acceptance tests

- Life tests