| Process ID | Process | Specification (Incl. Issue) | Description / Identification | Use and Location | User Code | Associated DML Items | Criticality of Process | Approval / Status |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Adhesive bonding | TBW Author: KW | Bonding of sensors into mounts and potting of wiring | Jiggle frame & structure & motor terminations | N/A | Eccobond 285 + catalyst 24LV, G-10, | medium | Identical to ID#17 |
|  | Adhesive bonding | TBW Author: KW | Bonding of flex-pivots into sleeves | Chop and Jiggle stage | N/A | inconel, Eccobond 285 + catalyst 24LV, aluminium 6082 | high | Confirmed by DM-1 warm shake |
|  | Adhesive bonding | N/A | Bonding of sleeves into housings | Chop and Jiggle stage | N/A | N/A | N/A | NOT USED |
|  | Adhesive bonding | TBW Author: KW | Harness tie-down | (TBD if required) | N/A | Eccobond 285 + catalyst 24LV, aluminium 6082 | low | Standard RAL practice. Used on BSM STM |
|  | Adhesive bonding | TBW Author: KW | fastener locking, | applied in visible location, eg under heads Applied to exposed threads and M2.5 nut holding launch lock base | N/A | Eccobond 285 + catalyst 24LV, aluminium 6082, stainless steel | medium | Standard RAL practice . Used as repair scheme on STM chop mirror screw |
|  | Adhesive bonding | TBW Author: KW | Bonding of magnets into pockets | Chop and Jiggle stage | N/A | Eccobond 285 + catalyst 24LV, aluminium 6082/6061, magnet | medium | Confirmed by DM-1 warm shake |
|  | Adhesive bonding | TBW Author: KW | Bonding of sensor actuators into pockets | Chop and Jiggle stage | N/A | Eccobond, aluminium 6082/6061, soft iron | medium | TBC. Similar process used on ISOPhot |
|  | Thermal stabilization | SPI-BSM-NOT-003 Author IP | Mirror stability cycling | Chop stage | N/A | Aluminium 6061 | high | ATC standard, adopted from NASA practice. |
|  | Electro-forming copper | Waveform Electroforming Ltd procedure EP/003-C iss2 | Manufacturing technique (sub-contract process) | Motor thermal shields | N/A | Electro formed Copper | medium | Confirmed by inspection and DM-1 warm shake |
|  | Gold plating 2-10 um | MOD DEF STAN 03-17/iss2 5 um thick | Plating (sub-contract process) | thermal contact, Emmisivity control | N/A | Gold, copper, nickel plate | medium | TBC |
|  | Niobium plating | N/A | Plating | Magnetic shielding | N/A | N/A | N/A | Not used |
|  | Alochrome | MOD DEF STAN: 03-18.iss2 To a light yellow appearance | Alocrom 1200 AL Alloy Surface Conversion | Corrosion control | N/A | Aluminium components where specified | low | Accepted RAL and ESA process. |
|  | Varnish application | Zeiss process | Coating | Insulation/ corrosion control | N/A | Not used | high | Zeiss motor coils have polyimid coating, but these are treated as bought-in components (see DCL) |
|  | Soldering | TBW Author BCG | Soldering | Connectors | N/A | Wiring, connectors, sensors, motors | high | ESA approved soldering practice |
|  | Crimping | TBC Author BCG | Crimping | Connectors | N/A | Wiring, connectors | high | TBD if required |
|  | Fastener Assembly | SPI-BSM-NOT-0018 V1.0 Author IP | Screw thread lubrication and torque control for BSM | BSM | N/A | All bolted components | High | An alternate MSSL procedure using apeizon-100 is also being considered |
|  | Bond Motors into housing | TBW: Author KW | Potting / bonding | Motor coils and their wires into G10 and Al housing, and | N/A | Eccobond 285 + catalyst 24LV Wiring, Zeiss coils, Aluminium 6082, G-10 | High | TBD |
|  | Cleaning before assembly | TBW: Author KW | Clean with ultrasound, IPA, tap water | After machining and before clean room acceptance | N/A | All | Medium | Similar to RAL cleaning process |
|  | Optical Surface cleaning | TBW, Author PTP | Clean with 'opti-clene' | BSM mirror, if required | N/A | BSM mirror | High | TBD |
|  | Optical Surface cleaning | TBW, Author PTP | Clean with IPA or acetone | BSM mirror, if required | N/A | BSM mirror | High | TBD |
|  | Optical Surface polishing | TBW, Author PTP | Abrasive clean with fine diamond paste | BSM mirror, if required (repair technique) | N/A | BSM mirror | High | TBD |
|  | Wiring routing | TBW, Author BCG | Wriring routing and tie down | BSM wiring harness | N/A | Wiring, connectors, P-Cips, lacing tape | Medium | TBD |
|  | Annealing | TBW, author TAP | Annealing of Brass P-clips | BSM wiring harness | N/A | Wiring | Low | TBD |