| BSM Material List ID | Component ID | Name & Type of Product, Form and Condition | Specification | Size Code | Processing Parameters | Outgassing SCC-Res. Data and Refer | OK to bake at 80°C? | Thermal & Vacuum stable? | OK at 4°K? | Manufacturer | Remarks, Approval Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Structure, Jiggle frame, Interface shoe, baffle | Aluminium plate, cold rolled. bar | 6082 | TBD | T6 (TBC) | TBD | Y | Y | Y | TBD |  |
|  | Baffle | Aluminium Sheet, welded. | 6082 | TBD | T6 (TBC) | TBD | Y | Y | Y | TBD |  |
|  | Mirror | Aluminium | 6061 | TBD | -T651 or T6511 | MSFC-HDBK-527F p88 Corrosion rating 'B'. | Y | Y | Y | TBD | Intermediate cycling per ATC Spec to provide stability. |
|  | Fasteners | stainless steel, | austenitic | N/A | TBD | TBD | Y | Y | Y | TBD |  |
|  | Locking inserts | stainless steel, | TBD | N/A | TBD | TBD | Y | Y | Y | TBD |  |
|  | Flex pivots | Inconel | 718 | N/A | TBD | TBD | Y | Y | Y | TBD | Austenitic stainless steel (304 grade) an alternative. |
|  | Flex pivot sleeves | stainless steel, aluminium or inconel TBD | TBD | TBD | TBD | TBD | Y | Y | Y | TBD |  |
|  | Sensor targets | Mild steel (Soft iron grade preferred – TBD | BS970 220M07 | TBD | TBD | TBD | Y | Y | Y | TBD | Corrosion protection by thin layer of varnish, material ID 19 |
|  | Sensor mount, motor housing | Glass fibre epoxy | G-10CR Or G10/40 (TBC) | TBD | TBD | TBD | Y | Y | Y | TUFNOL | TBC if required , may use aluminium instead. Note: A cryogenic grade material consisting of 7628 fabric woven with continuous e-glass fiber in an amine-cure |
|  | Potting compound/ Adhesive | Stycast | 2850FT | N/A | with Catalyst 11 | MAPTIS material 06451 | Y | Y | TBC | TBD | Various grades in MAPTIS, MSFC-HDBK. Select correct one NB - LIMITED LIFE MATERIAL |
|  | Adhesive, cable run | Eccobond | 285 | N/A | with catalyst 11 | MAPTIS database material 05475 | Y | Y | TBC | TBD | ATC practice is to use 286 - NB - LIMITED LIFE MATERIAL |
|  | Motor screening | Mu-metal, sheet 0.125mm thick | TBD | TBD | TBD | MSFC-HDBK-527F p181 (spec AMS 7701) Corrosion rating 'B' | TBC | TBC | TBC | Goodfellow | In MSFC HDBK as 'MAGNET HI-PERM-MUMETAL'. TBC if required |
|  | Harness - wire core | TBD | TBD | N/A | TBD | TBD | Y | Y | Y | TBD | Get space rated cable from RAL |
|  | Harness - insulation | TBD | TBD | N/A | TBD | TBD | Y | Y | TBC | TBD | Get space rated cable from RAL |
|  | Harness P-Clips | Brass | TBD | TBD | TBD | TBD | Y | Y | Y | TBD | TBC if required |
|  | Solder | Solder | TBD | N/A | TBD | TBD | Y | Y | Y | TBD | Space rated soldering certificate required |
|  | Motor Core | NiFe Soft magnentics Laminated sheets | ULTRA PERM 250 or CryoPerm 10 | TBD | TBD | TBD | Y (PACS) | Y (PACS) | Y (PACS) | TBD | Latest PACS paper says CryoPerm 10 |
|  | Motor Winding | Aluminium, high purity | 5N | TBD | TBD | TBD | Y (PACS) | Y (PACS) | Y (PACS) | California Fine Wires | TBC , may be 6N copper |
|  | Motor insulation | Varnish? | TBD | N/A | TBD | TBD | Y (PACS) | Y (PACS) | Y (PACS) | TBD | Zeiss, PACS approved |
|  | Motor winding frames | Vespel | SP-1 | TBD | TBD | TBD | Y | Y | Y | DuPont |  |
|  | Motor Permanent Magnet | NdFeB Permanent magnets | VACODYM 344 | TBD | TBD | TBD | TBC | Y (PACS) | Y (PACS) | TBD |  |
|  | Finish | QMW Black | Mk2 | N/A | TBD | TBD | TBC | Y | Y | TBD | TBD if required |
|  | Unfinished aluminium parts - TBD | Finish - anodize | TBD | N/A | TBD | TBD | Y | Y | Y | TBD | TBC if required |
|  | Thermal end stops | Copper (TBD) | TBD | TBD | TBD | TBD | Y | Y | Y | TBD | TBC if required |
|  | Surface plating | Copper flashing, Nickel Plate (TBD), Gold plate | TBD | N/A | TBD | TBD | Y | Y | Y | TBD |  |
|  | Motor Thermal shields | Copper | TBD | N/A | Electroformed | TBD | Y | Y | Y | TBD | Check electroformed Cu is OK |
|  | Magnetic Shielding | Niobium plate | TBD |  | plated | TBD | TBC | TBC | Y | TBD | Use as superconducting magnetic shield |