| BSM MatL ID | Part ID | Name & Type of Product, Form & Condition | Spec | Size Code | Processing Parameters | Corr | SCC | Flamm | Off-gas | Out-gas | OK to bake at 80°C? | Thermal & Vacuum stable? | OK at 4°K? | Manufacturer | Remarks, Approval Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Structure, Jiggle frame, Interface shoe, baffle | Aluminium SQUARE BAR | 6082 | To suit manuf | T6 BS L111 T6 Bar /BSL113 T6 Sheet / BS L114 T6 Tube / BSL 115 T6 Sheet | B | A | N/A | N/A | N/A | Y | Y | Y | ALCOA Extrusions | RAL DML list 1.01 composition Si 0.7-1.3, Fe 0.5, Cu 0.1, Mn 0.4-1, Mg 0.5-1.2, Cr 0.25, Ni 0.1, Zn 0.2, Ti 0.2 |
|  | Baffle | Aluminium Sheet, welded. | 6082 | N/A | T6 | B | A | N/A | N/A | N/A | Y | Y | Y | N/A | NOT USED : Baffle now machined as per material ID 1 |
|  | Mirror | Aluminium, Bar | 6061 | To suit manuf | -T651 | B | A | N/A | N/A | N/A | Y | Y | Y | British Al. Extrusions | Intermediate cycling per ATC Spec to provide stability. MSFC-HDBK-527F p88 ASTMB211 or ISO/UK equivalent |
|  | Fasteners | stainless steel, austenitic | A2-70 to DIN 267 | N/A | clean | A | A | A | N/A | N/A | Y | Y | Y | Reliance | Exact material within A2-70 per varies : ATC batch is traceable as AISI type 321 MAPTIS code: (10351, 10334, 10098) CRES 321) |
|  | Locking inserts | stainless steel, | A2-70 to DIN 267 | N/A | clean | A | A | A (GOX 500psi) | N/A | N/A | Y | Y | Y | Reliance | Exact material within A2-70 per varies : will be AISI type 304, 305 or 321. MAPTIS code: (10351, 10334, 10098) CRES 304, 321) |
|  | Deleted | INCONEL | 718 | To suit manuf | TBD | A | A | A | N/A | N/A | Y | Y | Y | SPECIAL METALS CORP / INCO ALLOYS INTL | Inconel not baselined - see material 4, 28, 29 for replacement. MAPTIS 55750, 10406 REFERS |
|  | Flex pivot sleeves | Aluminum plate, cold rolled. bar | 6082 | To suit manuf | T6 BS L111 T6 Bar /BSL113 T6 Sheet / BS L114 T6 Tube / BSL 115 T6 Sheet | B | A | N/A | U | N/A | Y | Y | Y | ALCOA or British Al. Extrusions | Baseline is Al 6082. As an option, may use matched grade material to flex pivots. |
|  | Sensor targets | Soft iron | R Fe 120 TO DIN 17405 | To suit manuf | ANNEAL | B? | B? | N/A | N/A | N/A | Y | Y | Y | VACUUMSCHMELZE GmbH | USED ON ISOPHOT CHOPPER Corrosion protection GOLD PLATING, |
|  | Sensor mount, motor housing | Glass fibre epoxy | G10/40 | Sheet, 1/4" thick | Machined | N/A | N/A | A | A | A | Y | Y | Y | TUFNOL | MAPTIS 02776 TML 0.51, CVCM 0.015 Note: A cryogenic grade material consisting of 7628 fabric woven with continuous e-glass fiber in an amine-cure |
| a | Potting compound/ Adhesive | Stycast | 2850FT | N/A | with Catalyst 11 | N/A | N/A | A | A TML <0.5 | A cvcm <0.02 | Y | Y | Y | Emerson & Cuming | Various grades in MAPTIS, MSFC-HDBK. Select correct one, EG 06451 NB - LIMITED LIFE MATERIAL |
| 10. b | Potting compound | Stycast | 2850FT | N/A | with Catalyst 9 | N/A | N/A | A | A TML <0.5 | A cvcm <0.02 | Y | Y | Y | Via TekData | Used in BSM cryoharness, supplied via RAL |
|  | Adhesive, cable run | Eccobond | 285 | N/A | with catalyst 11 | N/A | N/A | A | A TML <0.3 | A cvcm <0.03 | Y | Y | Y | Emerson & Cuming | MAPTIS 05475 NB - LIMITED LIFE MATERIAL |
|  | Deleted | Mu-metal, sheet 0.125mm thick | N/A | N/A | N/A | A | A | N/A | N/A | N/A | TBC | Y | TBC | Goodfellow | Deleted from Baseline design - MAPTIS code 10118 MSFC-HDBK-527F p181 (spec AMS 7701) Corrosion rating 'B' |
|  | Harness - wire core | Copper Alloy wire | ESA/SCC No.3901/013 | 21, 46 | See spec | N/A | N/A | See spec | Y | Y | Y | TekData | Supply via RAL, dpec SPIRE-RAL DOC-001362 |
|  | Harness - insulation | PTFE insulated wire | ESA/SCC No.3901/013 | 21, 46 | See spec | N/A | N/A |  | Y | Y | Y |  |  |
| a | Harness P-Clips, Motor shims | Brass shim, | CZ108 to BS2870, BSEN 1652:1998 CW508L | Sheet, | rotary sheared. | A | A | N/A | N/A | N/A | Y | Y | Y | RS Components | MAPTIS 10234 |
| 15.b | Jiggle frame Ballast mass, | Bar stock | CZ108 to BS2870, BSEN 1652:1998 CW508L | Bar | Annealed state | B | B | N/A | N/A | N/A | Y | Y | Y | TBC (via distributor) | MAPTIS 10321 |
|  | Solder | 66 Tin Solder, 96 tin solder (eutectic) | ECSS-Q-70-08A | N/A | N/A | TBC | TBC | TBC | TBC | TBC | Y | Y | Y | TBD | ESA Space rated soldering certification available. Option will be RAL solder (RAL DML 7.03) Multicore Alloy SN63 TIN/LEAD 22 SWG |
|  | Motor Core | NiFe Soft magnentics Laminated sheets | ULTRA PERM 250 or CryoPerm 10 | Sheet | Annealed | A | U | N/A | N/A | TBD | Y | Y | Y | Zeiss | All details with Zeiss/ PACS programme. DML V1.2: CryoPerm10 confirmed as selected. MAPTIS 10118 refers to similar material |
|  | Motor Winding | Aluminium, high purity | 5N | TBD | TBD | TBC | TBC | TBC | TBC | TBD | Y | Y | Y | California Fine Wires | All details with Zeiss/ PACS programme. |
|  | Motor insulation | Polyimid (sic) : Polyimide insulation | Per Zeiss/ PACS processes | N/A | Per Zeiss/PACS processes | TBC | TBC | TBC | TBC | TBD | Y | Y | Y | Zeiss (may be Dupont Kapton ?) | Grade and application technique not known (see Zeiss, PACS QA documents). |
|  | Motor winding frames | Vespel | SP-1 | TBD | TBD | TBC | TBC | TBC | TBC | TBD | Y | Y | Y | Zeiss, DuPont | Weight loss <10e-10 gm/cm²/s in -vacuum <500°F |
|  | Motor Permanent Magnet | NdFeB Permanent magnets | Grade 42 | 10mm dia | Ni Coated all faces |  |  |  |  | TBD | 80°C MAX | Y | Y | Magnet Sales UK | Ni plate for corrosion resistance, 15 microns thick all sides. Handle with care - powerful magnet. |
|  | deleted | QMW Black | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | Not used |
|  | deleted | Anodize | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | N/A | Alochrom added to DPL, deleted from DML |
|  | Thermal end stops | Copper | OHFC | N/A | Sheet BS 2875 C 103 | A | U | N/A | N/A | TBC | Y | Y | Y | TBC | TBC if required. MAPTIS 50836. RAL MATERIAL 2.06 |
|  | Surface plating | Copper flashing, Nickel Plate, | See DPL | N/A | See DPL | A | U | TBC | N/A | N/A | Y | Y | Y | MB Aerospace | SEE DECLARED PROCESS LISTs. MAPTIS 50141, 10311, 10328 |
|  | Motor Thermal shields | Copper | TBD | N/A | Electroformed | A | U | N/A | N/A | TBD | Y | Y | Y | Waveform Electro-forming | MAPTIS 10311. |
|  | Deleted | Niobium plate | N/A | N/A | plating | A | U | N/A | N/A | N/A | TBC | Y | Y | TBD | not baseline Potential use as superconducting magnetic shield, only if required by subsequent test . MAPTIS 50701 (wire) |
|  | Flex Pivots Jiggle (baseline) | Martensitic Stainless Steel | AISI 420 & 429 | To suit manufacture | TBC | B | U | A (GOX 750psi) | N/A | N/A | Y | Y | TBD | TBD | Included in Flex pivots (standard Lucas parts) - see Declared Component List. MAPTIS code 30136 (CRES 420) |
|  | Flex Pivots Chop (baseline) | Beryllium Copper | Uns 17200 | Various bar, sheet | Induction brazed, heat treated 600°F | A | U | N/A | N/A | N/A | Y | Y | Y | C-FLEX | Included in flex pivots (special C-Flex parts). MAPTIS 10271 |
|  | Plating, misc | Gold | See DPL | N/A | SEE DPL | A | A | N/A | N/A | N/A | Y | Y | Y | MB Aerosace. UK | MAPTIS 10328. SEE DPL FOR PLATING SPEC |
|  | Washer, Thermal compensation | INVAR 36, BAR (UNS K93601) | ASTM B753 Alloy T36 | 1/2" bar | Obtain in annealed state. | B | A | N/A | N/A | N/A | Y | Y | Y | Carpenter Techn. Corp. or Equiv | MAPTIS 10314. Gold plate for corrosion resistance |
|  | Grease | Apiezon Grease | Grade N | 25g tube | N/A | N/A | N/A | TBC | Vapour pressure <10-9 mbar a | TBC | TBC | Y | Oxford Instruments or equiv. | Melt point 43ºC, quantity small (screw threads on Cernox thermistor) and no running expected. |
|  | Motor lamination end terminations | Titanium | TBC | TBC | TBC | A | A | TBC | TBC | Y | Y | Y | Zeiss | All details with Zeiss/ PACS programme. |
|  | Lacing Tape | Dacron (unwaxed) | TBC | TBC | Clean before use | A | N/A | U | CVCM 0.02% | TML 0.35% | Y | Y | Y | Gudebrod Inc. 22DPTH NATURAL GUDE-SPACE PT Or equiv. | RAL DML ITEM 20.24 ESA-RD: 01 REV. 1 |