Herschel/SPIRE                                       SPIRE-MSS-PRJ-001129

MULLARD SPACE SCIENCE LABORATORY

| UNIVERSITY COLLEGE LONDON | Author: C BROCKLEY-BLATT |
| --- | --- |

SPIRE – STRUCTURE DECLARED MATERIALS

Document Number:  MSSL/SPIRE/PA002.1   29 November 2001

Distribution:

| Spire Project Office | B Winter |  |
| --- | --- | --- |
| ESA PX | A Heske |  |
|  | J Bruston |  |
|  | J Rautakoski |  |
| RAL | B Swinyard |  |
|  | K King |  |
|  | J Delderfield |  |
|  | J Long (Project Office) |  |
| Mullard Space Science Laboratory | A Smith |  |
|  | J Coker |  |
|  | C Brockley-Blatt |  |
|  | A Dibbens |  |
| ATC | C Cunningham |  |
|  | I Pain |  |
|  | T Paul |  |
| Cardiff | M Griffin |  |
|  | P Hargrave |  |
| JPL | J Bock |  |
|  | J Lilienthal |  |
| CEA | L Duband |  |
| Herschel Project | Herschel.Planck@esa.int |  |
| Author: | C Brockley-Blatt | Date: |  |
| Checked: | B Winter | Date: |  |
| Approved: | T Dibbens | Date: |  |

# Change Record

| ISSUE | Date | Brief description of change |
| --- | --- | --- |
| 0.1 | September 2001 | New document |
| 1.0 | November 2001 | Issued and Updated |

CONTENTS

Introduction



2.  Reference documents



3.  The Declared Materials Tables

# 1.   INTRODUCTION

This document identifies the material types that will be used in the SPIRE structure, as designed and built by MSSL.  The data is based on mature designs and is practically complete.
This document has been used to identify all the materials used by MSSL only.

2.   REFERENCE DOCUMENTS

## All documents are listed in Figure 3.2 of the CIDL.

3. THE DECLARED MATERIALS LISTS

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SPIRE/PA002.1 |
| --- | --- | --- |
| PROJECT: Herschel/SPIRE EXPERIMENT: EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 1. Aluminium and Aluminium Alloys |
| Itm No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 1. | Aluminium alloy 6082 | 6082-T6 Commercial product Extrusion/plate & rod | J Smith & Sons London UK BS 1470/1474 | Alocrom 1200 Chemglaze- Z306 Anodised- chromic acid |  | B | V | 3/4 | W4 |  |  |

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SPIRE/PA002 |
| --- | --- | --- |
| PROJECT: Herschel/SPIRE EXPERIMENT: EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 2. Copper and copper alloys |
| Itm No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 1. | Beryllium copper | Commercial product | Anderton Bradford, UK N 1400-0018 | N/A |  | B | V | 3/4 | W0 |  |  |

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SPIRE/PA002 |
| --- | --- | --- |
| PROJECT: Herschel/SPIRE EXPERIMENT: EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 4. Titanium and titanium alloys |
| Itm No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 1. | Titanium TI-6Al-4V | TI-6Al-4V, Ti alloy Commercial product 6STA Rod | Dornier |  |  | B | V | 3/4 | W2 |  |  |

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SPIRE/PA002 |
| --- | --- | --- |
| PROJECT: Herschel/SPIRE EXPERIMENT: EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 6. Stainless steels |
| Item No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 1. | Stainless steel AISI 321 | Commercial product AISI 321 S12/S20 | Various BS 1449 Barden Corp, Plymouth Devon, UK | N/A |  | B | V | 3/4 | W2 |  |  |

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SPIRE/PA002 |
| --- | --- | --- |
| PROJECT: Herschel/SPIRE EXPERIMENT: EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 7. Filler metals and solders |
| Itm No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 1. | Solder, Elsold | 63/37 Sn/Pb eutectic Rosin cored Commercial product Extrusion | Bleiwerk Goslar 63 tin solder eutectic as in ESA PSS-01-708 | Hand soldering of PCB's | All PCB's | B | V | 3/4 | W2 |  |  |

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SWT-UVOT/PA003 |
| --- | --- | --- |
| PROJECT: SWIFT EXPERIMENT: UVOT EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 10. Adhesives, coatings and varnishes |
| Itm No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 1. | Scotch Weld 1838 | Commercial product 2 part, epoxy adhesive | 3 M’s Adhesive Supplies | Mix 1:1 by mass Cure 4hrs @ 60°C | Secure magnets in dichroic assembly, | B | V | 3/4 | W1 |  |  |

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SPIRE/PA002 |
| --- | --- | --- |
| PROJECT: Herschel/SPIRE EXPERIMENT: EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 12. Paints, primers and inks |
| Itm No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 2. 3. 4. | Anodising Alocrom 1200 Chemglaze 9924 | Commercial product Chromic acid process Chromating Commercial product Polyvinyl butyral resin - Primer | Ingram & Glass, Godalming, UK DEF STN 0324 MSSL Hughson Chemicals US | N/A N/A N/A |  | B B B BB | V V V V | 3/4 3/4 3/4 3/4 | A3 A3 A4 |  |  |

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SPIRE/PA002 |
| --- | --- | --- |
| PROJECT: Herschel/SPIRE EXPERIMENT: EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 18. Thermoset plastics |
| Itm No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 1. | Vespel SP 1 | Polyimide Commercial product Unfilled base resin Bar | Du Pont USA Vespel SP 1 | N/A | High voltage xformer in Blue Module | B | V | 3/4 | W2 |  |  |
| 2. | Kapton | Polyimide tape Y966 acrylic adhesive coated. Commercial product | Du Pont USA (HPC Stevenage, UK) | N/A | Over heaters for thermal control etc | B | V | 3/4 | W1 |  |  |
| 3. | PTFE | PTFE Commercial product Plate | Du Pont USA | N/A | Spacers | B | V | 3/4 | W1 |  |  |
| 4. | Kapton H | Polyimide adhesive coated film | Du Pont | N/A | Xformer insulation in TMPSU | B | V | 3/4 | W0 |  |  |

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SPIRE/PA002 |
| --- | --- | --- |
| PROJECT: Herschel/SPIRE EXPERIMENT: EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 19. Wires and cables |
| Itm No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 1. | PTFE insulated copper wire | Pure PTFE coated, tin plated copper wire. Commercial product Single strand, shielded and twisted | Cabletec UK Filotex France ESA/SCC 3901/ 013 | Hand soldering Crimping |  | B | V | 3/4 | W4 |  |  |
| 2. | Enamelled conductor | Polyurethane coated copper wire | BICC Connollys UK BICOSOL, grade 2 also Alcatel-Copper | Fabrication of high voltage transformers & inductors |  | B | V | 3/4 | W2 |  |  |

| Issue No 1 | DECLARED MATERIALS LIST | MSSL/SPIRE/PA002 |
| --- | --- | --- |
| PROJECT: Herschel/SPIRE EXPERIMENT: EXPERIMENTER: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: A P Dibbens |
| CATEGORY: 20. Miscellaneous non-metallic materials |
| Itm No | Commercial Identification | Chemical Nature Type of Product Form & Condition | Procurement Info., Supplier Spec. Issue | Summary of Processing Parameters | Use & Location | Environmental Code R A T | Size Code | Approval Status | ESA Comments |
| 1. | Barden patented matl. Bartemp Bearings | Teflon coated glass fibres impregnated with MoS2 | Barden Corp Plymouth Devon UK | N/A |  | B | V | 3/4 | W1 |  |  |
| 2. | Duroid material | Duroid | SNFA Bearings, Glos. UK | N/A |  | B | V | 3/4 | W1 |  |  |
| 3. . | Gudebrod 450X | Lacing cord | Gudebrod Inc US | N/A |  | B | V | 3/4 | W1 |  |  |