Herschel – SPIRE Acceptance Data Package Flight Model Mirrors Fichier: LAM.QUA.SPI.ADP.030040_10_1.1_ADP FM mirrors .doc

| Prepared By : | Signature |
| --- | --- |
| Gérard ROUSSET PA/QA Date : 10/06/04 |  |
| Checked by : | Signature |
| Origne Alain Date :10/06/04 |  |
| Checked by : | Signature |
| Pascal Dargent Date : 10/06/04 |  |
| Approved by: | Signature |
| Dominique Pouliquen Date : 10/06/04 |  |

Change records

| Date | Edition | Révision | Modification | Pages concernées |
| --- | --- | --- | --- | --- |
| 27/12/03 | D | 0 | First release | All |
| 06/06/04 | 1 | 0 | Delivery to RAL |  |
| 09/06/04 | 1 | 1 | Section 12 : Main steps of the mirrors manufacture added Section 13 : Manufacture sheets available at LAM on request. |  |

Distribution List

| Institut | Name | Issue/Revision |
| --- | --- | --- |
|  |  | D- | 1/0 | 1/1 |  |  |  |  |  |  |  |
| CNES | Blanc Y. |  |  |  |  |  |  |  |  |  |  |
| CNES | Lorigny E |  |  |  |  |  |  |  |  |  |  |
| RAL | Griffin M.J. |  |  |  |  |  |  |  |  |  |  |
| RAL | King K.J. |  |  |  |  |  |  |  |  |  |  |
| RAL | Sawyer E. |  | X | X |  |  |  |  |  |  |  |
| RAL | Swinyard B.M. |  |  |  |  |  |  |  |  |  |  |
| CEA | Auguères J.L. |  |  |  |  |  |  |  |  |  |  |
| CEA | Cara C. |  |  |  |  |  |  |  |  |  |  |
| CEA | Tourrette T. |  |  |  |  |  |  |  |  |  |  |
| LAM | Baluteau J.P. |  |  |  |  |  |  |  |  |  |  |
| LAM | Bergès J.C. |  |  |  |  |  |  |  |  |  |  |
| LAM | Blanc J.C. |  |  |  |  |  |  |  |  |  |  |
| LAM | Boit J.L. |  |  |  |  |  |  |  |  |  |  |
| LAM | Bonnet D. |  |  |  |  |  |  |  |  |  |  |
| LAM | Castinel L. |  |  |  |  |  |  |  |  |  |  |
| LAM | Colin C. |  |  |  |  |  |  |  |  |  |  |
| LAM | Dargent P. |  |  |  |  |  |  |  |  |  |  |
| LAM | Dohlen K. |  |  |  |  |  |  |  |  |  |  |
| LAM | Ferrand D. |  |  |  |  |  |  |  |  |  |  |
| LAM | Jevaux M. |  |  |  |  |  |  |  |  |  |  |
| LAM | Levacher P. |  |  |  |  |  |  |  |  |  |  |
| LAM | Malina R. |  |  |  |  |  |  |  |  |  |  |
| LAM | Moreaux G. |  |  |  |  |  |  |  |  |  |  |
| LAM | Origné A. |  |  |  |  |  |  |  |  |  |  |
| LAM | Pouliquen D. |  | X | X |  |  |  |  |  |  |  |
| LAM | Rousset G. |  | X | X |  |  |  |  |  |  |  |
| LAM | Travers B. |  |  |  |  |  |  |  |  |  |  |

Table of contents

1	Shipping Documents	5

2	Transportation, Handling and Installation Procedures	1

3	Certificate of Conformance / Delivery review board MoM / AI list	1

4	Qualification status list / Test matrix	1

5	Interface Drawings	1

6	Mechanical drawings	1

7	As built configuration list	1

8	Serialised components list	1

9	List of Waivers	1

10	Copies of waivers	1

11	User manual	1

12	Historical record	1

13	Logbook / diary of events	1

14	Age sensitive Item record	1

15	Open Work / Deferred Work / Open tests	1

16	List of Non Conformance report	1

17	Copies of Non Conformance report	1

18	Test reports	1

19	Reference list of EIDP's	1

20	Mass records	1

21	Cleanliness statement	1

List of figures

Figure 1 Container 1	6

Figure 2 : Container 2	6

Figure 3 : Container 3	6

Figure 4 : Mirrors disposition inside the container 1	7

Figure 5 : Mirror disposition inside the container 2	7

Figure 6 : Mirror disposition inside the container 3	8

List of tables

Table 1: Container 1 - mirror list	5

Table 2: Container 2 - mirror list	5

Table 3 : Container 3 – mirror list	5

Table 4: List of mechanical drawings	1

Table 5 : As built configuration list	1

Table 6: Serial number of the FM mirrors	1

Table 7 : List of the Non-Conformances	1

Table 8 : List of test reports	1

# Shipping Documents

The delivered parts are the mirrors for the FM model of the spectrographic and photometric channels of the SPIRE instrument.

The mirrors are delivered in 3 containers:

- Container 1 contains  the following mirrors :

| Mirrors | Id Number | Used for |
| --- | --- | --- |
| SM7 | 03 | Spectrometer |
| SM12A | 02 | Spectrometer |
| SM12B | 02 | Spectrometer |
| PM10 | 02 | Photometer |
| PM11 | 03 | Photometer |
| TM | 02 | Witness mirror |

Table 1: Container 1 - mirror list

- Container 2 contains the following mirrors :

| Mirrors | Id Number | Used for |
| --- | --- | --- |
| CM3 | 03 | Photometer |
| CM5 | 02 | Photometer |
| PM6 | 02 | Photometer |
| SM6 | 02 | Spectrometer |
| SM8A | 03 | Spectrometer |
| SM8B | 03 | Spectrometer |
| SM11A | 03 | Spectrometer |
| SM11B | 02 | Spectrometer |
| TM | 03 | Witness mirror |

Table 2: Container 2 - mirror list

- Container 3 Contains  the following mirrors :

| Mirrors | Id Number | Used for |
| --- | --- | --- |
| PM7 | 03 | Photometer |
| PM8 | 02 | Photometer |
| PM9 | 01 | Photometer |
| SM9A | 02 | Spectrometer |
| SM9B | 01 | Spectrometer |
| SM10A | 03 | Spectrometer |
| SM10B | 02 | Spectrometer |
| TM | 06 | Witness mirror |

Table 3 : Container 3 – mirror list

The identification number is engraved on the rear part of the mirrors

A picture of the containers is given here after

Figure 1 Container 1

Figure 2 : Container 2

Figure 3 : Container 3

The disposition of the mirrors inside the container are given in the following figures :

Figure 4 : Mirrors disposition inside the container 1

Figure 5 : Mirror disposition inside the container 2

Figure 6 : Mirror disposition inside the container 3

# Transportation, Handling and Installation Procedures

List of provided procedures:

- Packing / Unpacking procedure  ref : LAM.QUA.SPI.PRC.031228_01_10

- SPIRE Mirrors - Mechanical mounting procedure : LAM.QUA.SPI.PRC.030015_10

# Certificate of Conformance / Delivery review board MoM / AI list

| Item : SPIRE Mirrors | CONFORMANCE | Doc. No : |
| --- | --- | --- |
| Model : FM |  |  |
| CERTIFICATE OF CONFORMANCE Herewith is certified that the delivered mirrors that will be used for the FM model of the SPIRE instrument and whose list is given in the section 1 of the present Acceptance Data Package, complies with the following documents : Spire Mirrors specification ref : LAM.PJT.SPI.SPT.200007 Ind 9 Definition drawings whose list is given in section 7 of this document. With the exception of the agreed ECR listed in the Section 16 of this ADP SPIRE Project Manager at LAM ___________________________ D. Pouliquen SPIRE Product Assurance at LAM ___________________________ G. Rousset |

# Qualification status list / Test matrix

Not Applicable

# Interface Drawings

For all the mirrors, the interface definition is given in the drawing : SPI.MIR.00.DI.01.A

# Mechanical drawings

List of provided drawings :

| Fore optics | Drawing ref: |
| --- | --- |
|  | CM3 | SPI-MIR-11-DD-01-A |
|  | CM5 | SPI-MIR-12-DD-01-A |
| Photometer Channel | Drawing ref: |
|  | PM6 | SPI-MIR-21-DD-01-A |
|  | PM7 | SPI-MIR-22-DD-01-A |
|  | PM8 | SPI-MIR-23-DD-01-A |
|  | PM9 | SPI-MIR-24-DD-01-A |
|  | PM10 | SPI-MIR-25-DD-01-A |
|  | PM11 | SPI-MIR-26-DD-01-A |
| Spectrometer Channel |  |
|  | SM6 | SPI-MIR-31-DD-01-A |
|  | SM7 | SPI-MIR-32-DD-01-A |
|  | SM8A | SPI-MIR-33-DD-01-A |
|  | SM8B | SPI-MIR-33-DD-02-A |
|  | SM9A | SPI-MIR-34-DD-01-A |
|  | SM9B | SPI-MIR-34-DD-02-A |
|  | SM10A | SPI-MIR-36-DD-01-A |
|  | SM10B | SPI-MIR-36-DD-02-A |
|  | SM11A | SPI-MIR-37-DD-01-A |
|  | SM11B | SPI-MIR-37-DD-01-A |
|  | SM12A | SPI-MIR-38-DD-01-A |
|  | SM12B | SPI-MIR-38-DD-01-A |

Table 4: List of mechanical drawings

# As built configuration list

The as built configuration list is given here after:

| Document | Doc reference |
| --- | --- |
| SPIRE Mirror Specification | LAM.PJT.SPI.SPT.200007 Ind 9 |
| ICD structure mechanical I/F | SPIRE-MSS-PRJ-000 Iss1-0 |
| I/F de montage des miroirs à 293K (Mirror mechanical I/F definition) | SPI.MIR.00.DI.01.A (Given in section 5) |

| Drawings |
| --- |
| Fore optics | Drawing ref: |
|  | CM3 | SPI-MIR-11-DD-01-A |
|  | CM5 | SPI-MIR-12-DD-01-A |
| Photometer Channel | Drawing ref: |
|  | PM6 | SPI-MIR-21-DD-01-A |
|  | PM7 | SPI-MIR-22-DD-01-A |
|  | PM8 | SPI-MIR-23-DD-01-A |
|  | PM9 | SPI-MIR-24-DD-01-A |
|  | PM10 | SPI-MIR-25-DD-01-A |
|  | PM11 | SPI-MIR-26-DD-01-A |
| Spectrometer Channel | Drawing ref: |
|  | SM6 | SPI-MIR-31-DD-01-A |
|  | SM7 | SPI-MIR-32-DD-01-A |
|  | SM8A | SPI-MIR-33-DD-01-A |
|  | SM8B | SPI-MIR-33-DD-02-A |
|  | SM9A | SPI-MIR-34-DD-01-A |
|  | SM9B | SPI-MIR-34-DD-02-A |
|  | SM10A | SPI-MIR-36-DD-01-A |
|  | SM10B | SPI-MIR-36-DD-02-A |
|  | SM11A | SPI-MIR-37-DD-01-A |
|  | SM11B | SPI-MIR-37-DD-01-A |
|  | SM12A | SPI-MIR-38-DD-01-A |
|  | SM12B | SPI-MIR-38-DD-01-A |

Table 5 : As built configuration list

# Serialised components list

Serial number of the delivered FM components:

| Mirrors | Id Number |
| --- | --- |
| CM3 | 03 |
| CM5 | 02 |
| PM10 | 02 |
| PM11 | 03 |
| PM6 | 02 |
| PM7 | 03 |
| PM8 | 02 |
| PM9 | 01 |
| SM10A | 03 |
| SM10B | 02 |
| SM11A | 03 |
| SM11B | 02 |
| SM12A | 02 |
| SM12B | 02 |
| SM6 | 02 |
| SM7 | 03 |
| SM8A | 03 |
| SM8B | 03 |
| SM9A | 02 |
| SM9B | 01 |
| TM (1) | 02 |
| TM (1) | 03 |
| TM (1) | 06 |

Table 6: Serial number of the FM mirrors

(1) Witness mirror (one per container)

# List of Waivers

No RFW issued

# Copies of waivers

Not applicable

# User manual

The mirrors will be aligned with the help of the document " SPIRE Optical alignment plan ref: LAM.OPT.SPI.PRC.030023_10.

This documents is given here after

# Historical record

The overall operations implemented on the mirrors, from the material incoming inspection to the packing, are traced in the "manufacture sheets" which are not provided in this document, but available at LAM on request.

However, the main steps of the mirror manufacture are given here after:

- Rough machining of the blanks

- Thermal cycling for material relaxation

- Final machining of the blanks

- Metrology of the blanks

- Surface treatment (Alodine 1200)

- Optical surface manufacture by diamond turning

- Metrology of the optical surface

- Cleaning

- Optical verification of the optical surface (Interferograms, roughness)

- Bake out

# Logbook / diary of events

The deliverables being individual parts, there is no logbook. For each mirror, the traceability is given in the "manufacture sheets" which are not deliverables but available at LAM on request.

# Age sensitive Item record

Not applicable

# Open Work / Deferred Work / Open tests

No Open work, deferred work, open tests

# List of Non Conformance report

The list of non conformances is given in the table at the following sheet:

| DATE | NCR ref | MIN/MAJ | Parts designation | Reference document | NCR Title | STATUS C/O |
| --- | --- | --- | --- | --- | --- | --- |
| 21/08/2002 | LAM.QUA.SPI.NCR.020016 | MIN | SM12 b # 02 | SPI-MIR-37-DD-01-A | Thermal treatment posponed after the finishing | C |
| 21/08/2002 | LAM.QUA.SPI.NCR.020022 | MIN | SM12 a # 02 | SPI-MIR-37-DD-01-A | Thermal treatment posponed after the finishing | C |
| 21/08/2002 | LAM.QUA.SPI.NCR.020030 | MIN | SM8 b # 03 | SPI-MIR-33-DD-02-A | Thermal treatment posponed after the finishing | C |
| 21/08/2002 | LAM.QUA.SPI.NCR.020032 | MIN | CM5 # 02 | SPI-MIR-12-DD-01-A | Thermal treatment posponed after the finishing | C |
| 21/08/2002 | LAM.QUA.SPI.NCR.020036 | MIN | PM7 # 03 | SPI-MIR-22-DD-01-A | Thermal treatment posponed after the finishing | C |
| 25/11/2002 | LAM.QUA.SPI.NCR.020068 | MAJ | CM5 #1,2,3 | SPI-MIR-12-DD-01-A | Width of the mirror is too short by 1 mm ( 160 instead of 161) | C |
| 25/11/2002 | LAM.QUA.SPI.NCR.020074 | MIN | CM5 #1,2,3 | SPI-MIR-12-DD-01-A | New alodine treatment after repair and striping of the first treatment | C |
| 25/11/2002 | LAM.QUA.SPI.NCR.020076 | MIN | SM11 A et SM 11 B # 1,2,3 | SPI-MIR-37-DD-01-A | New alodine treatment after repair and striping of the first treatment | C |
| 17/01/2004 | LAM.QUA.SPI.NCR.040117_01 | MAJ | PM6 # 02 | SPI-MIR-21-DD-01-A | Default on radius of curvature | C |
| 17/01/2004 | LAM.QUA.SPI.NCR.040117_02 | MAJ | SM6 # 02 | SPI-MIR-31-DD-01-A | Default on radius of curvature | C |
| 17/01/2004 | LAM.QUA.SPI.NCR.040117_03 | MAJ | SM8A # 03 | SPI-MIR-33-DD-01-A | Default on radius of curvature | C |
| 17/01/2004 | LAM.QUA.SPI.NCR.040117_04 | MAJ | SM8B # 03 | SPI-MIR-33-DD-02-A | Default on radius of curvature | C |
| 23/01/2004 | LAM.QUA.SPI.NCR.040123_01 | MAJ | PM6 # 02 | SPI-MIR-21-DD-01-A | Default on radius + shift of the centre of curvature | C |
| 23/01/2004 | LAM.QUA.SPI.NCR.040123_02 | MAJ | SM6 # 02 | SPI-MIR-31-DD-01-A | Default on radius + shift of the centre of curvature | C |
| 23/01/2004 | LAM.QUA.SPI.NCR.040123_03 | MAJ | SM8A # 03 | SPI-MIR-33-DD-01-A | Default on radius + shift of the centre of curvature | C |
| 23/01/2004 | LAM.QUA.SPI.NCR.040123_04 | MAJ | SM8B # 03 | SPI-MIR-33-DD-02-A | Default on radius + shift 3Zof the centre of curvature | C |
| 23/01/2004 | LAM.QUA.SPI.NCR.040123_05 | MAJ | SM11A # 03 | SPI-MIR-37-DD-01-A | Shift of the centre of curvature | C |
| 23/01/2004 | LAM.QUA.SPI.NCR.040123_06 | MAJ | SM11B # 02 | SPI-MIR-37-DD-01-A | Shift of the centre of curvature | C |
| 18/02/2004 | LAM.QUA.SPI.NCR.040218_01 | MAJ | SM9A # 02 | SPI-MIR-34-DD-01-A | Default on radius of curvature | C |
| 18/02/2004 | LAM.QUA.SPI.NCR.040218_02 | MAJ | SM9B # 01 | SPI-MIR-34-DD-02-A | Default on radius of curvature | C |
| 18/02/2004 | LAM.QUA.SPI.NCR.040218_03 | MAJ | SM10A # 03 | SPI-MIR-36-DD-01-A | Default on radius of curvature | C |
| 18/02/2004 | LAM.QUA.SPI.NCR.040218_04 | MAJ | SM10B # 02 | SPI-MIR-36-DD-02-A | Default on radius of curvature | C |
| 10/03/2004 | LAM.MEC.SPI.NCR.040319_01 | MAJ | All the PFM Mirrors | LAM.PJT.SPI.SPT.200007 Ind 9 | Roughness of the optical surface of the mirrors | C |
| 25/05/2004 | LAM.QUA.SPI.NCR.040525_01 | MAJ | CM5_02 | SPI-MIR-12-DD-01-A | Shift of the centre of curvature | C |
| 25/05/2004 | LAM.QUA.SPI.NCR.040528_01 | MAJ | CM5_02 | SPI-MIR-11-DD-01-A | Thickness of the mirror | C |
| 25/05/2004 | LAM.QUA.SPI.NCR.040528_02 | MAJ | CM3_03 | SPI-MIR-11-DD-01-A | Thickness of the mirror | C |

Table 7 : List of the Non-Conformances

# Copies of Non Conformance report

See the Non Conformance Report at the following sheet

# Test reports

The test report list is given in the table here after:

| Document title | Document reference | Status |
| --- | --- | --- |
| Mass measurement report | LAM.QUA.SPI.PRV.040116_01_10 | Delivered (See Doc in Section 20) |
| SPIRE FM mirrors - Optical measurement report | LAM.QUA.SPI.PRV.040118_01_10 | Delivered |
| SPIRE FM mirrors – Mechanical I/F measurement report | LAM.QUA.SPI.PRV.040117_01_10 | Delivered |

Table 8 : List of test reports

# Reference list of EIDP's

Not applicable

# Mass records

The mass and CdG measurement report is given in the document. " SPIRE Mirrors, Mass and CoG measurement report " ref : LAM.QUA.SPI.PRV.040116_01 Ed1 Rev 0 .

# Cleanliness statement

The delivered mirrors have been cleaned according to the procedure LAM.QUA.SPI.PRC.020047_10, they have been baked out at 75° during 48h at a pressure of 10-5 Torr, according to the procedure LAM.QUA.SPI.PRC.030010_10.