Herschel/SPIRE

MULLARD SPACE SCIENCE LABORATORY

| UNIVERSITY COLLEGE LONDON | Author: C Brockley-Blatt |
| --- | --- |

SPIRE – STRUCTURE DECLARED PROCESSESS LIST

Document Number:  MSSL/SPIRE/PA004.06   September 2005

Distribution:

| Spire Project Office | B Winter |  |
| --- | --- | --- |
| ESA PX |  |  |
| RAL | B Swinyard |  |
|  | K King |  |
|  | E Sawyer |  |
|  | J Long (Project Office) |  |
| Mullard Space Science Laboratory | A Smith |  |
|  | J Coker |  |
|  | C Brockley-Blatt |  |
|  | A Spencer |  |
| ATC |  |  |
| Cardiff | M Griffin |  |
|  | P Hargrave |  |
| JPL | J Bock |  |
| CEA | L Duband |  |
| Herschel Project | Herschel.Planck@esa.int |  |
| Author: |  | Date: |  |
| Checked: |  | Date: |  |
| Approved: |  | Date: |  |

Change Record

| ISSUE | DATE |  |
| --- | --- | --- |
| 0.1 | September 2001 | New document |
| 2 | 22 November 2002 | Issued |
| 3 | January 2003 | Updated with Silver Soldering |
| 4 | March 2003 | Updated to remove processes not used |
| 5 | June 2004 | Updated to include new processes, 6 – 10. |
| 6 | September 2005 | Updated to include new processes |

Table of Contents

- Scope of Document

- Applicable and Reference Documents

- Declared Processes List

# Glossary

All terms are listed in the CIDL.

1	Scope of Document

This document presents all the processes to be used all along the design, development and manufacture of the structure for SPIRE.  This includes the Level 0 and 300mK thermal strap subsystems.

# 2.	Applicable and Reference Documents

## All documents are listed in Figure 3.2 of the CIDL.

## Declared Processes List

The Structure Declared Processes List, which consists of multiple arrays of 10 columns which shall be completed as indicated in AD04, is presented here below:

Processes should be grouped in the table below:

| Group Type | Used |
| --- | --- |
| 1. Adhesive Bonding | ( |
| 2. Composite Manufacturing | ( |
| 3. Encapsulation/Molding | N/A |
| 4. Painting/Coating | ( |
| 5. Cleaning | ( |
| 6. Welding/Brazing | ( |
| 7. Crimping/Stripping/Wire Wrapping | ( |
| 8. Soldering | N/A |
| 9. Surface Treatment | N/A |
| 10. Plating (Allo-chroming) | ( |
| 11. Machining | ( |
| 12. Forming | ( |
| 13. Heat Treatment | ( |
| 14. Special Fabrication | N/A |
| 15. Marking | ( |
| 16. Miscellaneous Processes | N/A |
| 17. Inspection Procedure | ( |

| Issue No 6 | DECLARED PROCESSES LIST |  |
| --- | --- | --- |
| PROJECT: HERSCHEL EXPERIMENT: SPIRE EXPERIMENTERS: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: C Brockley-Blatt |
| Itm No | Process | Specification | Description/ identification | Use and location | User code | Associated DML items | Criticality of process | Approval Status | Project Sign Off | ESA Sign Off | ESA Comments |
| 1. | Stycast 2850 FT Black | Commercial 2 part epoxy adhesive for cryogenics |  | Internal and external wiring harness supports | MSSL | 10-02 | Non-critical |  |  |  |  |
| 2. | Crimp connections | ECSS-Q-70-26 | Fabrication of wiring harnesses | Internal and external wiring harnesses | MSSL | 19-01 | Non-critical |  |  |  |  |
| 3. | Alocrom 1200 | MOD 03-18 | Chromating - Commercial process | Various | MSSL | 01-01,02, 01-03 | Non-critical |  |  |  |  |
| 4. | Heat Treatment T 73 | Mil-H-6088-F | Thermal treatment | Treatment for aluminium | SNL | 01-01 | Non-critical |  |  |  |  |
| 5 | Silver Soldering | MSSL In-House Procedure | Brazing using a 55% silver solder (rest is zinc, copper and Tin) | Thermal joints on the thermal bus bar | MSSL | 07-01 | Non-critical |  |  |  |  |
| Issue No 6 | DECLARED PROCESSES LIST |  |
| PROJECT: HERSCHEL EXPERIMENT: SPIRE EXPERIMENTERS: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: C Brockley-Blatt |
| Itm No | Process | Specification | Description/ identification | Use and location | User code | Associated DML items | Criticality of process | Approval Status | Project Sign Off | ESA Sign Off | ESA Comments |
| 6. | Goldplating | RAL Procedure 10 μm Soft Gold |  | Level 0 Thermal Straps and 300mK busbar | Rutherord Appleton Laboratories, Chilton | 10-02 | Non-critical |  |  |  |  |
| 7. | Composite Manufacture | In-house Procedure | Fabrication of FPU and detector box mounts | FPU and detector box mounts | B3 Technologies Shalford | 15-01, 15-02 | Non-critical |  |  |  |  |
| 8. | Compression welding | In-House Procedure | Welding under pressure and heat (nominally 900 deg C) | Level 0 Thermal Straps | EMS, Germany | 02-01, 02-02 | Critical |  |  |  |  |
| 9. | Electron Beam Welding | In House Procedure | Stake welds at 1mm wide by 13.5mm | Level 0 Thermal straps | EBP, Woking | 02-01, 02-02 | Critical |  |  |  |  |
| 10. | Glue Joint Isolation | In house-procedure - MSSL-MEG-PRC-2003-01. | Electrical isolation | Thermal Straps | MSSL | 02-01, 02-02 10-01 | Non-critical |  |  |  |  |
| Issue No 6 | DECLARED PROCESSES LIST |  |
| PROJECT: HERSCHEL EXPERIMENT: SPIRE EXPERIMENTERS: MULLARD SPACE SCIENCE LABORATORY (MSSL) PREPARED BY: C Brockley-Blatt |
| Itm No | Process | Specification | Description/ identification | Use and location | User code | Associated DML items | Criticality of process | Approval Status | Project Sign Off | ESA Sign Off | ESA Comments |
| 11. | Vacuum Annealing | UKAEA Specification (Ref MSSL CV268689) | UKAEA Vacuum Annealling | Level 0 Thermal Straps and 300mK Bus bar | UKAEA, Dept. of Special Techniques, Culham Science Centre | 02-02, 02-03, 02-04 | Critical |  |  |  |  |