Inspection & Test Report

SPIRE PCal Candidate Sources

SPIRE Ref.: SPIRE-UCF-

Cardiff Ref.: HSO-CDF-RP-095

09 June 2004

Prepared by: Peter Hargrave, Iris Didschuns

Approved by:

Distribution list

# Details

## HBI-1

Flight-like source with full redundancy. Sapphire substrate. Wires are brass and with indium solder. Film impedance too low for flight.

## HBI-2

Flight-like source with full redundancy. Sapphire substrate. Wires are brass and with indium solder. Film impedance too low for flight.

## HBI-3

Flight-like source with full redundancy. Sapphire substrate. Wires are brass and with indium solder. Film impedance too low for flight.

## HBI-4

Flight-like source with full redundancy. Sapphire substrate. Wires are brass and with indium solder. Film impedance too low for flight.

## HBI-5

Flight-like source with full redundancy. Sapphire substrate. Wires are brass and with indium solder. Film impedance acceptable for flight.

## HBI-6

Flight-like source with full redundancy. Sapphire substrate. Wires are brass and with indium solder. Film impedance acceptable for flight.

## HBI-7

Flight-like source with full redundancy. Sapphire substrate. Wires are brass and with indium solder. Film impedance acceptable for flight.

## HBI-8

Flight-like source with full redundancy. Sapphire substrate. Wires are brass and with indium solder. Film impedance acceptable for flight.

# Incoming inspection

## HBI-1

Figure 2-1 HBI-1 - prime source

Figure 2-2 HBI-1 – Redundant source

## HBI-2

Figure 2-3 HBI-2 - prime source

Figure 2-4 HBI-2 – Redundant source

## HBI-3

Figure 2-5 HBI-3 - prime source

Figure 2-6 HBI-3 – Redundant source

## HBI-4

Figure 2-7 HBI-4 - prime source

Figure 2-8 HBI-4 – Redundant source

## HBI-5

Figure 2-9 HBI-5 – Prime source

Figure 2-10 HBI-5 – Redundant source

## HBI-6

Figure 2-11 HBI-6 – Prime source

Figure 2-12 HBI-6 – Redundant source

## HBI-7

Figure 2-13 HBI-7 – Prime source

Figure 2-14 HBI-7 – Redundant source

## HBI-8

Figure 2-15 HBI-8 – Prime source

Figure 2-16 HBI-8 – Redundant source

# Device impedances

values in brackets are measured by two-wire-method with a handheld multimeter FLUKE?

## HBI-1

#### 10/06/04

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source | 125.82 | 124.98 | 125.22 | 125.97 |
| redundant source | 132.52 | 130.57 | 130.41 | 132.44 |
| CX25830 | 42.01 | 118.14 | 891.12 |  |

the warming up (4K to 300K) was constantly monitor and the data file can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-1_test_no_29\HBI-1_thermal_10_06_04.txt

#### 14/06/04

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source | 126.03 | 125.19 | 125.21 | 125.99 |
| redundant source | 132.48 | 130.60 | 130.42 | 132.46 |
| CX25830 | 41.85 | 118.04 | 885.31 | 41.95 |

the warming up (4K to 300K) was constantly monitor and the data file can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-1_test_no_29\HBI-1_thermal_14_06_04.txt

#### 16/06/04

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source | 126.12 | 125.22 | 125.33 | 126.08 |
| redundant source | 132.55 | 130.59 | 130.49 | 132.46 |
| CX25830 | 41.77 | 118.13 | 929.2 | 41.97 |

the warming up (4K to 300K) was constantly monitor and the data file can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-1_test_no_29\HBI-1_thermal_16_06_04.txt

#### 28/06/04

open cryostat and remove HBI-1 source

## HBI-2

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source |  |  |  |  |
| redundant source |  |  |  |  |

## HBI-3

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source |  |  |  |  |
| redundant source |  |  |  |  |

## HBI-4

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source |  |  |  |  |
| redundant source |  |  |  |  |

## HBI-5

IMAGES – HBI-5-P, HBI-5-R, HBI-5-ALL

resistance measured with a handheld multimeter (two-wire)

| 27/07/04 | 300K (() |
| --- | --- |
| prime source | 200.44 |
| redundant source | 211.28 |

#### 25/08/04

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source | 200.4 (200.44) | 188.8 | 188.78 | 200.4 |
| redundant source | 211.1 (211.28) | 200.1 | 200.43 | 211.1 |

- cooling cryostat to LN2 temperature and later to LHe temperature

- taking dark current and power/time constant measurements, the data file can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\\HBI-5_test_no_32\

#### 26/08/04

- top-up LHe

- taking dark current and power/time constant measurements, the data file can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-5_test_no_32\

#### 01/09/04

- open cryostat and remove HBI-5, RCX25830=42.12 (

## HBI-6

| 27/07/04 | 300K (() |
| --- | --- |
| prime source | 198.11 |
| redundant source | 201.4 |

#### 06/09/04

- HBI-6 mounted in clean room to DM structure, ready for characterisation at 4K.

#### 08/09/04

- mounted inside the test cryostat and put on to the pump

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source | 199.2 | 189.2 | 189.8 | 199.26 |
| redundant source | 201.1 | 190.5 | 191.0 | 201.2 |

#### 09/09/04

cooling down to LN2 temperature

cooling down to LHe temperature

taking dark current and power/time constant measurements, the data file can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-6_test_no_33\

#### 10/09/04

top-up LN2 and LHe

finish time constant and power measurements, the data file can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-6_test_no_33\

let the system warming up

## HBI-7

| 27/07/04 | 300K (() |
| --- | --- |
| prime source | 209.1 |
| redundant source | 194.1 |

#### 16/09/04

HBI-7 mounted into the cryostat

#### 17/09/04

cooling down to LN2 temperature

cooling down to LHe temperature

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source | 211.7 | 201.2 | 201.8 | 211.9 |
| redundant source | 194.3 | 184.4 | 184.7 | 194.2 |

carrying out time constant and power measurements, the data file can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-7_test_no_34\

let the system warming up

#### 21/09/04

open cryostat and remove HBI-7

#### 23/11/04

HBI-7 mounted inside the cryostat and put on the pump

#### 24/11/04

cooling down to LN2 temperature

cooling down to LHe temperature

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source | 212.3 | 201.6 | 202.1 | 212.2 |
| redundant source | 194.9 | 184.9 | 185.1 | 194.8 |

carrying out time constant and power measurements in more detail, the data can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-7_test_no_39\

let the system warming up

#### 06/12/04

open cryostat and remove HBI-7

## HBI-8

| 27/07/04 | 300K (() |
| --- | --- |
| prime source | 192.9 |
| redundant source | 193.9 |

#### 23/09/04

cooling down to LN2 temperature

cooling down to LHe temperature

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source | 192.4 | 182.6 | 183.0 | 192.61 |
| redundant source | 191.9 | 182.2 | 182.66 | 113.24 |

#### 24/09/04

carrying out time constant and power measurements, the data files can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-8_test_no_35\

the redundant source shows a short and a lower impedance before running the test

let the system warming up

#### 26/10/04

remove temporally the source to try to find the short – nothing

mount inside the cryostat, no short could be detected but still lower impedance

cooling down to LN2 temperature

cooling down to LHe temperature

|  | 300K (() | 77K (() | 4.2K (() |
| --- | --- | --- | --- |
| prime source | 192.9 | 182.97 | 183.37 |
| redundant source | 111.86 | 98 | 96.02 |

carrying out time constant and power measurement prier to the life test, the data can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-8_test_no_36\

start life test, the data can be found: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\life test\HBI-8\

#### 29/10/04

finish life test

carrying out time constant and power measurements after the life test, the data can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-8_test_no_37\

let the system warming up

#### 01/11/04

|  | 300K (() |
| --- | --- |
| prime source | 193.3 |
| redundant source | 111.97 |

#### 15/11/04

cooling down to LN2 temperature

cooling down to LHe temperature

|  | 300K (() | 77K (() | 4.2K (() | 300K (() |
| --- | --- | --- | --- | --- |
| prime source | 193.12 | 183.24 | 183.7 | 193.13 |
| redundant source | 111.92 | 98.05 | 96.06 | 111.91 |

carrying out time constant and power measurement in more detail, the data can be found in: \\Darkstar\Astroworld\Projects\Spire\Cardiff_workpackages\PCAL\Assembly&test\PFM\HBI-8_test_no_38\

let the system warming up

#### 23/11/04

open cryostat and remove HBI-8

# Historical records

## HBI-1

| Date | Event | Comments |
| --- | --- | --- |
| 09/06/04 | Installed in Pcal structure for photodetector tests | Wiring aperture sealed with aluminium tape. |
| 10/06/04 | Installed in the Cryostat and Cryostat cool down |  |
| 10/06/04 | Photodetector tests commence |  |
| 10/06/04 | Cryostat warming up |  |
| 14/06/04 | Cryostat cool down |  |
| 16/06/04 | Swap wires between prime and redundant source |  |

## HBI-2

| Date | Event | Comments |
| --- | --- | --- |

## HBI-3

| Date | Event | Comments |
| --- | --- | --- |

## HBI-4

| Date | Event | Comments |
| --- | --- | --- |

## HBI-5

| Date | Event | Comments |
| --- | --- | --- |
| 27/07/04 | Source acceptance checks |  |
| 11/08/04 | Source mounted into DM structure ready for photometric tests | Mounted in clean room, bagged, taken to clean-air cabinet in lab for integration to test dewar. |
| 12/08/04 | Installed in the cryostat |  |
| 25/08/04 | cryostat cool down to LHe and start taking measurements |  |
| 26/08/04 | finish measurements and let cryostat warming up |  |
| 05/09/04 | remove from cryostat |  |

## HBI-6

| Date | Event | Comments |
| --- | --- | --- |
| 27/07/04 | Source acceptance checks |  |
| 08/09/04 | Installed in the cryostat |  |
| 09/09/04 | cooling system to LHe temperature and start taking measurements |  |
| 10/09/04 | finish measurements and let cryostat warming up |  |
| 13/09/04 | remove source from cryostat |  |

## HBI-7

| Date | Event | Comments |
| --- | --- | --- |
| 27/07/04 | Source acceptance checks |  |
| 15/09/04 | Source mounted ready for tests |  |
| 16/09/04 | Installed in the cryostat |  |
| 17/09/04 | cooling system to LHe temperature, start taking measurements and let cryostat warming up |  |
| 21/09/04 | remove source from cryostat |  |
| 23/11/04 | Installed in the cryostat |  |
| 24/11/04 | cooling system to LHe temperature, start taking measurements and let cryostat warming up |  |
| 06/12/04 | remove source from cryostat |  |

## HBI-8

| Date | Event | Comments |
| --- | --- | --- |
| 27/07/04 | Source acceptance checks |  |
| 22/09/04 | Source mounted ready for tests |  |
| 23/04/09 | Installed in the cryostat cooling system to LHe |  |
| 24/09/04 | cooling system to LHe temperature and start taking measurements | when 0.25mW applied to redundant source the control program showed wrong value (0.02mW), checked program – it’s ok; check set-up with Pcal dummy – it’s ok; check Pcal impedance – not ok only have of the original value; check for shorts – YES |
| 27/09/04 | remove source from cryostat |  |
| 26/10/04 | Installed in the cryostat cooling system to LHe and start taking measurements | redundant shows no short to GND but still wrong impedance |
| 26/10/04 | start life test of primary source only |  |
| 29/10/04 | finish life test of primary source, start taking measurements and let cryostat warming up |  |
| 15/11/04 | cooling system to LHe temperature, start taking measurements and warming the cryostat | redundant shows no short to GND but still wrong impedance |
| 23/11/04 | remove source from cryostat |  |

# Test results

## Time constants

The time constants are measured after the illuminator is turned on and off, for various illuminator power levels. These are referred to as rising and falling time constants, respectively.

## Power

# Safety Measures

# Environmental Conditions

# Test Organisation (Personnel/Responsibilities

# Test Results

# Conclusions